## Slide 1: Development of ESPEI: free energy minimization, phase diagram calculations for multicomponent systems
Richard Otis and Zi-Kui Liu
Penn State University
May 14, 2015

## Slide 2
G. B. Olson, 2013
Focus for workshop (phase-based property data needed to build
Composition, temperature, pressure dependent CALPHAD-base databases

## Slide 3: CALPHAD Data Challenges
Data fragmentation
Data standards
Workflow tools
Uncertainty quantification
Reproducibility

## Slide 4: Maintaining CALPHAD Databases
C. E. Campbell, U. R. Kattner and Z. K. Liu, "The development of phase-based property data using the CALPHAD method and infrastructure needs,“ Integrating Materials and Manufacturing Innovation, Vol.3, 2014, 12.

## Slide 5: Goals of ESPEI
Workflow tools for CALPHAD modeling, including integration with FP calculations
Online APIs for accessing structured CALPHAD data and metadata
Open-source (MIT license) implementations of all core routines for CALPHAD, including
  Phase/property diagrams
  Fitting experimental data (CALPHAD modeling)

## Slide 6: pycalphad
First public release April 2015
5000 lines of code
800 code commits in 2 years
Interactive (shown) and non-interactive modes

## Slide 7: pycalphad
Up to 32 degrees of freedom per phase
TDB file support
Plotting: binary diagrams work best for now
Experimental ternary support
All standard alloy models (R-K-M polynomials, IHJ magnetic, order-disorder)
Available on Python Package Index and GitHub https://github.com/richardotis/pycalphad

## Slide 8: Reproducible CALPHAD Assessments
Jupyter/IPython Notebook
  Free and open-source software for interactive computing, based on Python
  Browser-based interface but can run locally
  Number-crunching power of MATLAB (NumPy) and symbolic math power of Mathematica (SymPy)
  Shen, H. (2014). Interactive notebooks: Sharing the code. Nature, 515(7525), 151–2. doi:10.1038/515151a

## Slide 9: Reproducible CALPHAD Assessments

## Slide 10: Demo
Al-Zn and Al-Mg assessment
Uncertainty quantification of parameters
Towards Al-Mg-Zn automated assessment

## Slide 11: Advantages of Python Approach
Notebook files are just text files
  Can be stored in version-control software
Better than a macro file: figures and text embedded in notebook
Supplementary material in journal articles
  Acts as interactive manuscript outline
  Others can easily reproduce your work

## Slide 12: Conclusion and Future Work
pycalphad 0.2 is coming soon
  New equilibrium engine, better fitting routines
Online CALPHAD Data API (Materials Genome, Inc.)

## Slide 13
Thank You
rao140@psu.edu
https://github.com/richardotis/pycalphad
This work is sponsored by a NASA Space Technology Research Fellowship under grant number NNX14AL43H.

## Slide 14: Open-source CALPHAD codes
OpenCalphad v2
Written in Fortran
GPL license
Interactive: TC-style macros
Non-interactive: TQ API
Very fast
Modeling module planned
pycalphad 0.2-pre
Written in Python
MIT license
Interactive: Python
Non-interactive: Python
Very flexible
Experimental modeling support