## Slide 1
SANS BASICS
Boualem Hammouda
National Institute of Standards and Technology
Center for Neutron Research
hammouda@nist.gov

## Slide 2: OUTLINE
1. The SANS Technique
2. SANS Data Analysis
    Standard Plots (Guinier, Porod, Guinier-Porod)
  SANS Models
  Inverse Fourier Transform, Shape Reconstruction Method
3. SANS Research Topics
A- Core-Chain Model for PMMA-P3HT
B- Polymer Co-solvation and Co-nonsolvation
C- Single-Chain Conformations in PNIPAM Solutions
4. Final Points
  USANS and VSANS
  Final Words

## Slide 3: 1 – The SANS Technique

## Slide 4: The NIST Old Guide Hall

## Slide 5
The NIST New Guide Hall

## Slide 6: Small-Angle Neutron Scattering
Incident Beam
Area Detector
Scattered
Beam
Sample
Q
Source
Aperture
Sample
Aperture
Monochromatic
Neutron Beam
Monochromation
Collimation
Scattering
Detection
neutron
wavelength
scattering
angle

## Slide 7: Nanoscale Structures
0.01
0.001
0.1
1
Scattering Variable Q (Å-1)
Length Scale (Å)
100
1000
10
10-4
10-5
104
105
106
Polymers
Complex
Fluids
Biology
SANS
USANS
VSANS

## Slide 8
COHERENT
INCOHERENT
Q-independent
no info. about structure
~ Contrast factor = (rA-rB)2
- Info. about structure
Scattering length density:
SANS Cross Sections

## Slide 9
Zero contrast
Multiple contrasts
Contrast match
Finite contrast
The Contrast Match Method

## Slide 10: 2 –SANS Data Analysis

## Slide 11
Standard Plots (Guinier Plot, Porod Plot, Guinier-Porod)
SANS Models
Inverse Fourier Transform, Shape Reconstruction Method
SANS Data Analysis

## Slide 12
Guinier-Porod Regions
Guinier Plots

## Slide 13: The Guinier-Porod Model
Continuous function
and derivative

## Slide 14: The Generalized Guinier-Porod Model
Continuous function
and derivative
s = 0 sphere
s = 1 cylinder
s = 2 plates

## Slide 15: SANS Models
volume
fraction
contrast
factor
Macromolecules
Particles
Structure
Factor
SI(Q)
Form
Factor
P(Q)
Structure
Factor
SI(Q)
Form
Factor
P(Q)
form
factor
structure
factor
Random Phase Approximation
Ornstein Zernike
particle
volume
cross
section

## Slide 16: Particle Structure Factor – The Ornstein-Zernike Equation
U(r)
r
Hard Sphere
Screened Coulomb
Square Well
Form
Factor
P(Q)
Structure
Factor
SI(Q)

## Slide 17: Fourier Transform
r
r’
R
Fourier transform:
Radial pair correlation function:
Density-density correlation function:

## Slide 18
Shape Reconstruction and
Inverse Fourier Transform
Homochiral
Heterochiral
Heterochiral
Homochiral
Shape Reconstruction
Fiber cross sections
Inverse Fourier
Transform

## Slide 19
A- Core-Chain Model for PMMA-P3HT
B- Polymer Co-solvation and Co-nonsolvation
C- Single-Chain Conformations in PNIPAM Solutions
3. SANS Research Topics

## Slide 20
A- Core-Chain Model for PMMA-P3HT

## Slide 21: The Core-Chain Model
uniform
core
grafted
polymer
chain
Term1
Term2
Term3
Term4
Four contributions:
Core-core Term1
Chain-chain Term2
Core-chain Term3
Chain-core-chain Term4
Note that one can recover the following limits: simple core, simple chain, and star-branched polymer.

## Slide 22: Radius of Gyration for Core-Chain Structures
Radius of gyration depends on the neutron scattering length densities.
Guinier Law

## Slide 23: PMMA – P3HT Core-Chain Structure
PMMA – P3HT Core-Chain
Results:
R = 10.3 nm,
Np = 4
Nm = 216
a = 0.6 nm
= 0.78
Rg = 37.6 nm
PMMA
P3HT

## Slide 24: The Empirical Core-Chain Model
Note that approximating the scattering by the sum of two functions for the core (Term1) and the chain (Term2) neglects the cross terms (Term3 and Term4).

## Slide 25: B- Polymer Co-solvation and Co-nonsolvation

## Slide 26
mixed phase
(1-phase)
phase
separated (2-phase)
composition
T
e
m
p
LCST
LCST
phase
separated (2-phase)
mixed phase
(1-phase)
composition
T
e
m
p
UCST
UCST
Polymer Demixing Phase Transitions
Temperature
I(0)
I(0)
Temperature
Upper Critical Solution Temp.
Lower Critical Solution Temp.

## Slide 27
PNIPAM in d-ethanol/d-water Mixtures
UCST
LCST

## Slide 28
PEO in d-ethanol/d-water Mixtures
UCST
LCST

## Slide 29
MIX
ING
Z
O
N
E
PEO in d-ethanol/d-water Mixtures

## Slide 30
Co-solvation and Co-nonsolvation
UCST
LCST
d-water
T
e
m
p
Co-solvation
M
I
X
I
N
G
Z
O
N
E
d-ethanol
PEO
LCST
UCST
T
e
m
p
Co-nonsolvation
NO MIX
Z
O
N
E
d-water
d-ethanol
PNIPAM

## Slide 31
PNIPAM in d-ethanol/d-water Mixtures

## Slide 32
PNIPAM in d-ethanol/d-water Mixtures
NO MIX
ZONE

## Slide 33
- Most polymers dissolve better in solvent mixtures (cosolvation)
- PNIPAM obeys a co-nonsolvation rule
- PEO is characterized by a “perfect” solvation window for 10 % d-water.
- PNIPAM is characterized by a non-solvation window for 60 % d-water.
- SANS is a valuable thermodynamic probe to study phase transitions as well as nanostructures
Results

## Slide 34: C- Single-Chain Conformations in PNIPAM Solutions

## Slide 35
PNIPAM in d-Water
Scattering Intensity (cm
-1
)

## Slide 36
SANS is valuable for measurements of single-chain conformations even in non-dilute polymer samples
d/h polymers dissolved in d/h solvents
D2O/H2O contrast variation series yields the zero average contrast condition
The zero average contrast sample yields single-chain conformations (with no inter-chain contributions)
The Zero Average Contrast Method

## Slide 37
SANS Scattering Cross Section
The Zero Average Contrast Method
Equal degrees of polymerization for d and h polymers
d polymer h polymer solvent
Single-chain
form factor
Contrast
factor
Inter-chain
contributions
zero average contrast

## Slide 38
1
9
13
14
15
16
hPNIPAM
dPNIPAM
d-water
2
3
4
5
6
7
8
10
11
12
50
%/50%
h-water
Predicted
ZAC
4 % PNIPAM h/d Samples Prepared
4% PNIPAM in water

## Slide 39
Contrast Variation Series
d-Water Fraction

## Slide 40
Zero Average Contrast Sample
Scattering Intensity (cm
-1
)
Scattering Variable Q (Å-1)

## Slide 41
Apparent and Single-Chain Rgs
Radius of Gyration (Å)

## Slide 42
PNIPAM/water is characterized by two effects:
PNIPAM/water phase separates (LCST) (apparent Rg increases)
PNIPAM single-chains collapse (single-chain Rg decreases)
Results

## Slide 43: 4. Final Points

## Slide 44: Upgrade and VSANS
30 m SANS
Old Guide Hall
New Guide Hall
30 m SANS
40 m VSANS
10 m SANS
USANS
Confinement
Building
USANS Instrument

## Slide 45: SANS, VSANS and USANS Ranges
VSANS
SANS
USANS

## Slide 46: Final Words
  THE SANS PROGRAM AT NIST
  SANS Instruments: two 30 m, one 10 m, New 40 m VSANS
Collaborators: He Cheng, Man-Ho Kim and Mike Hore
http://www.ncnr.nist.gov/staff/hammouda/
  SANS Q&A Kahoot
  http://www.kahoot.it/
  enter pin
  first name