## Slide 1: Diffusion and Relaxation in Cooled Liquids and Heated Crystalline Materials
Jack Douglas, NIST
Francis Starr, Wesleyan University
Beatriz Betancourt (NIST)
Hao Zhang, University of Alberta

## Slide 2
Beatriz Pazmiño Betancourt Polymer Thin Films and Nanocomposites, NIST
Francis Starr
Physics Department
Wesleyan University
Hao Zhang Department of Chemical and Materials Engineering, University of Alberta

## Slide 4
The transport properties of cooled liquids
such as the self-diffusion coefficient, shear viscosity, and structural relaxation times are typically non-Arrhenius over a large T range.
Log 
Tg / T
m
   exp [D T0 / (T –T0)]
Volgel-Fulcher-Tammann
Equation
Tg  (2/3) Tm

## Slide 5
TTammann  (2/3) Tm
Reduced Variables-
Enhanced Potential
Tranferability?

## Slide 7: Something to Bear in Mind in Relation to the Relevance of this Phenomena to Metallurgical Interests apart from Metallic Glasses and Melt Processing
The high surface-to-volume ratio of “nanostructured materials” such as nanoparticles, fabricated nanostructures, nanograins of polycrystalline solid metal materials (additive manufacturing context) by virtue of the Gibbs-Thompson effect:
Tm = Tm(bulk) - # (a /) ,  = characteristic confinement length
Au nanoparticles
CdSe
NPs
PRA 13,2287 (1976)
Simulation Ni NPs
ACS Nano 8, 7465
(2014)

## Slide 8
Recently, both simulations and experiments have revealed that the dynamics of diverse condensed ‘amorphous’ materials at equilibrium are characterized by significant heterogeneity in the local mobility and by a progressively increasing collective motion upon cooling that takes the form of string-like collective particle rearrangements linked to
the rate of structural
relaxation and diffusion.

## Slide 9: What this means in practice is that the lines between hard and soft matter science start to become Blurred  Conceptual approaches from complex fluids, especially polymer fluids, begin to take on great relevance to describing the transport properties of metallurgical materials  Study of metallurgical materials can give great insights into the dynamics of polymer materials- Really!

## Slide 10: Tune Liquid Dynamics by Varying Structure of Fluid Molecule, Confinement, Additives, Pressure Polymers Are Great Model Systems For This Type of Study!

## Slide 11: Thin Polymer Films
Riggleman et al., PRL 97, 045502 (2006)

## Slide 12: Polymer Nanocomposites

## Slide 13: FENE Polymer Model
Equilibrium molecular dynamics simulatin of a dense polymer melt
400 chains of 20 monomers each (un-entangled)
Fixed density ρ = 1.0 / Constant pressure
Wide temperature range: 0.30 < T < 2.5 (TA /  ≈ 0.7, Tc /  ≈ 0.35)
non-bonded
monomers
r
V
bonds
frustration /glass formation
Approximate mapping to real units
  Monomer size ≈ 1 nm to 2 nm
  Interaction strength  ≈ 1 kJ / mol
  Tg ≈ 100˚C

## Slide 14
Some Basic Properties: Pure Polymer Melt
“Decoupling”- FSE
Structural relaxation time

## Slide 15
Comparison of Simulations to VFT Relation
Betancourt et al.
PNAS 112, 2966 (2015)

## Slide 16: Adam-Gibbs Model / RFOT
Physical argument / three assumptions:
Relaxation is an activated process associated with local
particle motions at high temperatures and cooperative particle rearrangements associated with the precipitous drop in the configurational entropy, sc.
2) The activation energy Ea for long wavelength structural relaxation is extensive in the mass L of the dynamic particle clusters (CRR) that are the physical expression
of cooperativity, Ea ~ L. Pretty vague about their form!
Thermodynamic Connection
3) L ~ 1 / sc . Bigger clusters - larger , fragility  L(T)

## Slide 17: Thermally Activated Transport

## Slide 18
Activated Dynamics at High Temperatures
Still not really understood much beyond Eyring arguments
Riggleman et al., PRL 97, 045502 (2006); JCP 126, 234903 (2007); PRE 76, 011504 (2007)
Coarse-Grained Polymer Melt

## Slide 19: Cooperative Molecular Motion and Relaxation

## Slide 20: Quantifying Collective Motion
Pronounced asymmetry of distribution indicates that it is more probable for a mobile particle to move in the direction of another mobile particle than any other direction,
‘strings’

## Slide 21: Cooperative Motion in Glass-Forming Liquids
Donati et al., PRL 80, 2338 (1998); Cond Matt 9706277v1
Binary LJ mixture
‘Strings’
L

## Slide 22
“Decoupling”
“Fractional Stokes-Einstein Relation”
D / T ~ (1/)1 - 
  0.29  0.03

## Slide 23: Cooperativity and Adam-Gibbs Model Dynamic clusters involving cooperative motion growing in scale upon cooling or upon increasing concentration in particle suspensions can be directly observed b Phenomenon seems to be universal, even more general than glass-forming liquids!
Weeks

## Slide 24: Dynamic Heterogeneity: Polymer Melt
Mobile
Immobile

## Slide 25: Mobile and Immobile Particle Clusters
Mobile, M
Immobile, I

## Slide 26: Mobile and Immobile Particle Clusters- Equilibrium Branched Polymers
Immobile, I
Mobile, M

## Slide 27: Elastic Constant Fluctuations in Glass

## Slide 28: String-like Cooperative Motion in Polymer Melt

## Slide 29: Strings in the Pure Polymer Melt

## Slide 30: Strings are Self-Avoiding Polymers

## Slide 32
( )

## Slide 33: Polymer Nanocomposites
Betancourt, Hanakata, Starr, Douglas, PNAS , March issue (2015))

## Slide 34
String-like Collective Dynamics in the
Dynamics of Crystal Interfaces

## Slide 35: Physical Aging

## Slide 36: Entropy-Enthalpy Compensation

## Slide 37: Entropy-Enthalpy Compensation in Polymer Films
Slope defines the “Compensation
Temperature” Tcomp ≈ 0.18
Tcomp ≈ T0 of bulk polymer?

## Slide 38
Ni Diffusivity / Different X’stal Interfaces
Activation energy and pre-factors for
different surfaces are nicely compensated
See also: Boisvert et al., PRL 75, 469 (1995) ; Papageorgiou
and Evangelakis, Surface Science 461, L-543 (2000)

## Slide 39: “Strings” - Ubiquitous Form of Collective Excitation in Condensed Matter

## Slide 40: Cooperative Motion in the Glassy Grain Boundaries of Polycrystalline Materials
Zhang et al., PNAS 106, 7735 (2009)
Granular fluid - PRE
81, 041301(2010)
Expt: Ganapathy et al., PNAS (2011)

## Slide 41: Cooperative Motion on NP Surfaces
Ni Nanoparticle (2 nm) / catalytic temperature range
Zhang, Kalvapalle and Douglas, Soft Matter 6, 5944 (2010)

## Slide 42
String-like Collective Dynamics in the
Dynamics of Crystal Interfaces
Also:
Cu-Zr
metallic
glasses

## Slide 43
Collective Motion in Melting and Freezing
J. Phys. Chem. B, 115, 14068 (2011)

## Slide 44
Special issue on glass-forming liquids - online

## Slide 45
String-like Collective Dynamics in the Atomic
Motions of Membranes?

## Slide 46
String-like Collective Dynamics in the Atomic
Motions of Proteins ?
ubiquitin
T= 277 K

## Slide 47: Conclusions  The problem of understanding the dynamics of liquids, and other forms of strongly interacting non-crystalline matter (“Soft Matter”) is a central difficulty in many materials design applications, especially those involving elevated temperatures and nanostructured materials  Simulations on a wide range of materials indicate that a general type of excitation exists in non-crystalline materials (“strings”) whose significance for diverse forms of Soft Matter might be comparable to dislocations, and other lattice defects, in their influence on the properties of crystals.

## Slide 48: Basic Problem: How to determine string length? Dynamic Heterogeneity Mobility fluctuations Mobility fluctuations should imply ‘noise’ ???? New Finding: 1/ f or ‘colored noise’ having a power  is related to string length, L = <n>. Zhang and Douglas , Glassy Interfacial Dynamics of Ni Nanoparticles: Parts I – II, Soft Matter (2013)
breathers

## Slide 51: Particle and additive induced changes in crystallization morphology
Nature Materials 2, 92 (2003)
Nature Materials 3, 645 (2004)
See also for block copolymers: Phys. Rev. Lett. 99, 216101 (2007)
PRE 72, 011605 (2005)
Spherulites
PRE 65, 051606 (2002)

## Slide 52
Relaxation, free volume, elasticity
and collective motion
Different faces of same coin ? PNAS (March Issue)

## Slide 53: Andrade Creep Universal Property of Condensed Amorphous Matter
J(t)
t, sec
Struik
T  Tg