## Slide 1: MGI: Putting an End to Alloy Oops:* NEED DATA
C. E. Campbell, U.R. Kattner, E. Lass,
Metallurgy Division, NIST
And
Laura Bartolo, Kent State University
*Doug Foxvog, ITL

## Slide 2: Materials Data for the MGI
Initial Data &Tools development will focus on thermodynamics, kinetics and other phase-based material properties.
Future work will build on this experience and expand into other areas.
Microstructure Prediction Tools
Processing Modeling Tools
Materials Properties
Prediction Tools
Designed New Material
Material Optimizer
Error propagation/
Uncertainty Analysis
Material Performance Criteria
Data Generation & Storage Tools
Need to develop and curate materials information databases is well established.

## Slide 3: Why Start with Thermodynamics, Kinetics and Phase-based Material Properties
Gibbs energy | 
Entropy | 
Enthalpy | 
Heat capacity | 
Chemical potential | 
Volume | 
Thermal expansion | 
Isothermal compressibility | 
Bulk modulus | 
Intrinsic diffusivity | 
a
b
L
Gibbs Energy
Composition
T<TE
A
B
B2
g
Al Mole Fraction Ni Ni
(Ni)
Ni3Al
Annealed microstructure
As cast microstructure

## Slide 4: Data Generation & Storage Tools
First Principles
CALPHAD
DATA
(Experimental and Calculated)
Atomistic Simulations
Tools: e.g. CMS
Reference Data
Notes: The specific part of the materials design challenge we would like to tackle first. DATA!!! (This is experimental and calculated data). How can we make better use of the data available and avoid having repeat data reviews everytime we want to change a model or add new experimental. What is the best data for a given system?
Additional goals: making CALPHAD, Atomistic simulations, and first principles calculations more self-consistent.

## Slide 5: Need for File Repository
A-B-C-D-E-F
(ABCDEF.TDB)
A-B-C
A-D-E
A-D-F
C-D-E
B-E-F
B-D-E
B-D-E
B-C-D
A-B-E
B-C-E
B-C-F
A-C-F
A-B-D
A-B-E
A-B-F
A-C-D
A-C-E
C-D-F
C-E-F
D-E-F
A-B
A-D
A-C
C-D
C-F
C-E
B-D
B-F
B-E
A-E
B-C
A-F
D-E
E-F
D-F
A
B
C
D
E
F

## Slide 6: Structure of CALPHAD Database Files
Functional Descriptions
(e.g. TDB files)
Evaluated Data Files
(e.g. POP, DOP)
Thermodynamic
Descriptions
Thermodynamic Data
Database(s)
Unary
Binary
Ternary
…
Multi-comoponent
Diffusion Mobility Descriptions
Molar Volume
Descriptions
Diffusion Data
Molar Volume Data
…
Other Data

## Slide 7: Examples of Files for a CALPHAD Diffusion Mobility Assessment
Database files
Evaluated Data Files (e.g.DOP)
Link to associated TDB file
Elements: e.g. A,B
Phases: e.g. FCC_A1 and BCC_A2 (crystal structure)
Software/version used (e.g. TC-PARROT, ver S)
Reference info for data
    Bibliographic info, DOI link
Author info
  Name
  Reference info
    Bibliographic info, DOI link
Author info
    Name, e-mail
  User Comments
  Links to other files
MACRO/Script files (e.g. to run simulations , DCM)
Elements
Phases
Reference
Author
Links to other files (grid data, start values)
User comments
Note: Thermo-Calc based file extensions used, but information on file types should also be included
Thermodynamic Description
Link to TDB file or
reference
Diffusion Mobility Description
Elements: e.g. A,B
Phases: e.g. FCC_A1 and BCC_A2 (crystal structure)
Software/version used
Reference info
    Bibliographic info
    DOI link
Contributor info
    Name
    E-mail
  User Comments
  Links to other files
Auxiliary data files
(e.g. *.EXP)
Link to POP and/or TDB
Elements
Phases
Reference info
Author
User comments
Links to other files
Linked to
Searchable interface
Notes: Types of files used in CALPHAD assessment process.
The TDB file is an ASCII file describing the composition, temperature, pressure dependent Gibbs energy functions (for a phase diagram description). It could also be an ASCII file describing the composition and temperature dependence of the diffusion mobilities.
The POP and DOP files are text files that describe the experimental data used in assessment. The format is specific to the optimizing software.
The EXP (experimental files) files used when plotting the experimental results. The MACRO files are just text files used to run a simulation for a particular calculation.

## Slide 8: Data Generation & Storage Tools
First Principles
CALPHAD
Atomistic Simulations
DATA
(Experimental and Calculated)
Tools: e.g. CMS
Reference Data
Notes: The specific part of the materials design challenge we would like to tackle first. DATA!!! (This is experimental and calculated data). How can we make better use of the data available and avoid having repeat data reviews everytime we want to change a model or add new experimental. What is the best data for a given system?
Additional goals: making CALPHAD, Atomistic simulations, and first principles calculations more self-consistent.

## Slide 9: Data Generation & Storage Tools
First Principles
CALPHAD
Atomistic Simulations
DATA
(Experimental and Calculated)
Tools: e.g. CMS
Reference Data
Notes: The specific part of the materials design challenge we would like to tackle first. DATA!!! (This is experimental and calculated data). How can we make better use of the data available and avoid having repeat data reviews everytime we want to change a model or add new experimental. What is the best data for a given system?
Additional goals: making CALPHAD, Atomistic simulations, and first principles calculations more self-consistent.

## Slide 10: Computational Methods and Data
Input data for parameter development
First principles
Atomistic simulations
CALPHAD
Data for verification

## Slide 11: Information Need to Describe General Data Entry
Data
Elements present
Type of value (e.g. enthalpy, heat of formation, phase boundary, diffusivity, lattice parameter, bulk moduli)
  Experimental or computational method
  Type of measurement (direct or indirect)
Number of phases present
Datum value and error
  Type (single value or series)
  Units
  Actual value(s) and error(s)
For each phase present
  Phase name
  Composition and fraction and errors
  Crystal structure (this input will follow the format prescribed by the CCN) or amorphous
  Lattice parameter
Temperature and error
Pressure and error
Metadata
Type of material
  Bulk composition
  Material purity
  Sample preparation
  Microstructure information
    Single crystal
    Polycrystalline (grain size, dislocation density)
    Non-crystalline
Data manipulation details (if any, e.g. reference state corrections, analysis method to determine interdiffusion coefficient)
Reporting format (raw data, digitized data, other)
Reference (DOI or text ; one must be present)
Additional information
Need flexible formats that can evolve with changing data needs!

## Slide 12: Identifiers
Crystal Structure
  Materials consist of distinct phases which are characterized by their crystal structures.
  Crystallographic data (lattice parameter(s), space group symmetry, positional parameters) for a phase convey the identities of constituent atoms as well as their exact positions in space.
  Information on the identities and arrangement of constituent atoms (crystallographic data) provide the initial critical input for modeling materials behavior.
  Use the InChI identifier (Space group & wycoft sites)
Material (Composition, Heat Treatment, + ???
  InChI type identifier

## Slide 13: Diffusion Data Types
Tracer Diffusivity
Intrinsic Diffusivity
Interdiffusion
Grain boundary diffusion
Activation Energies
Diffusion Couple Composition Profiles
Layer widths
Could be reported as a function or individual determined diffusivites .
Need to know temperature, composition, phases, present, and diffusing species
Metadata Need:
Type of material
  Bulk composition
  Material purity
  Sample preparation
  Microstructure information
    Single crystal
    Polycrystalline (grain size, dislocation density)
    Non-crystalline
Data manipulation details (if any, e.g. reference state corrections, analysis method to determine interdiffusion coefficient)
Reporting format (raw data, digitized data, other)
Reference (DOI or text ; one must be present)
Additional information

## Slide 14: Things to Consider
Naming conventions for files
  ABC_Smith05.xxx
Files to reproduce a specific DICTRA simulation store together in a zip or separate linked files in workspace

## Slide 15: Concepts for Workspace/Workflow
An individuals can have multiple different workspaces.
  AlCu-Thermodynamics; CoNi-Diffusion, ReNi-Experimental. AlTi-FirstPrinciples
Owner of the workspace defines who has access to the workspace and what the level of access is.
Workspaces can be shared between different groups/worskspaces
Workspaces would have some basic structure elements specific to the type of workspace.
  Thermodynamics, Diffusion, Experiments (types of workspace)
  Common structural elements: People, Types of Resources, Systems

## Slide 16: Discussion Points – What’s workable?
- Naming conventions for files & workspaces
- Files to reproduce a specific DICTRA
- Some files stored in zip; others as separate linked files
- Start with 8 categories:
  People; Phased Based Materials Properties; Phases; Software; Systems; Techniques; Treatments; Types of Resources

## Slide 17: File Repository for ATAT-MAPS Data Structure
Chemical Systems:
Au-Cu, NaCl-KCL, SiC-AlN, AlN-GaN-InN, …
System
Notes
Figures
Structures
Figures
Figure 1
Figure 2
…
Structures
Structure 1
Structure 2
...
Structure n
Structure 1
Condition 1
Condition 2
…
Structure 2
Condition 1
Condition 2
…
…
Structure n
Condition 1
Condition 2
…

## Slide 18: Original CALPHAD Approach
Experimental phase diagram and thermochemical data
Determine Gibbs energy functions for each phase: G = f (x,T,P)
Calculated phase
diagram
A
B
TE
a
Liquid
b
Temperature
Composition
A
B
TE
a
Liquid
b
Temperature
Composition
Binaries
Ternaries
Quaternaries
nth Order
Systems
True quaternary compounds are rare in metallic systems
Assessment of ternary systems is usually sufficient for the description of a multicomponent system
Same methodology can be applied to the description of other property data
a
b
L
Gibbs Energy
Composition
T<TE
A
B