## Slide 1
Development of CALPHAD descriptions for Ti-6Al-4V alloys
Greta Lindwall1, Kil-Won Moon1, Zhangqi Chen2,
Michael Mengason1, Justin Gorham1, Peisheng Wang1,
Ursula Kattner1 and Carelyn Campbell1
1NIST, Gaithersburg MD
2The Ohio State University, Columbus OH
September 11, 2017

## Slide 2: Motivation
10 µm
0
200
400
600
800
1000
0
20
40
60
80
α
β
α + β
Temperature (°C)
Mass fraction vanadium (%)
600-700 °C
900 °C
Ti 6-4 composition (ASTM B348 grade 5)
Ti 5.5-6.75 Al 3.5-4.5 V max 0.2 O max 0.3 Fe
Typical for Electron Beam Melting (EBM)
Build platform – heated to 700°C
Powder – preheated
Hot Isostatic Pressing (HIP): 900°C for 2 h
Phase diagram Ti-6Al + V
HIPed microstructure
10 µm
As-built microstructure
Materials provided by
Hrabe et al., NIST Boulder
10 µm
Ti 6-4

## Slide 3: Objectives
10 µm
0
200
400
600
800
1000
0
20
40
60
80
α
β
α + β
Temperature (°C)
Mass fraction vanadium (%)
600-700 °C
900 °C
Ti 6-4 composition (ASTM B348 grade 5)
Ti 5.5-6.75 Al 3.5-4.5 V max 0.2 O max 0.3 Fe
Typical for Electron Beam Melting (EBM)
Build platform – heated to 700°C
Powder – preheated
Hot Isostatic Pressing (HIP): 900°C for 2 h
Phase diagram Ti-6Al + V
Ti 6-4
10 µm
This work aims to…
Develop CALPHAD descriptions of
the diffusion mobilities for the α and β phases in the Ti-Al-V system
the thermodynamics of the Ti-Al-V-O system
10 µm
0
500
1000
1500
2000
2500
Temperature (°C)
0
5
10
15
20
25
30
35
Mass fraction oxygen (%)
α
β
liquid
halite
Ti3O2
α-TiO
Ti2O3
Phase diagram Ti-O

## Slide 4: Outline
Available diffusion data for Ti-Al-V
Thermodynamics of the Ti-Al-V System
  Influence of oxygen
Diffusion couple experiments
Diffusion mobility modeling
Summary and future work

## Slide 5: Al-V-Ti Diffusion in the Literature
β (bcc)
Li et al. (2002)
Ghosh et al. (2002)
Q. Chen (2004) (unpublished)
Wang et al. (2010) (no parameters)
Huang et al. (2010)
Y. Chen (2014)
J. Tran (2009)
α (hcp)
Q. Chen (2004) (unpublished)
J. Tran (2009)
Calphad Mobility Assessments

## Slide 6: Ti-Al + O
700
800
900
1000
1100
1200
1300
1400
1500
0
1
2
3
4
5
6
7
8
9
10
Temperature (°C)
β + α
β
α
Mass fraction Al (%)
+ 0.05 wt% O
0
1
2
3
4
5
6
7
8
9
10
β + α
β
α
α +
Ti3Al
Mass fraction Al (%)
+ 0.5 wt% O
Addition of O increases the 2-phase α + β region…
…and stabilizes Ti3Al (ordered hcp) at lower Al concentrations
2-phase region
1-phase region
Experiments
Calculations
current modeling
α +
Ti3Al
Mass fraction Al (%)
1
2
3
4
5
6
7
8
9
10
β + α
β
α
+ 1.0 wt% O
α +
Ti3Al
0

## Slide 7: Ti-V + O
calculated using
current model
α region
β region
α + β region
phase boundary
Experiments
Solubility ( ) measured on ultra-high purity materials
Molokanov et al. (1977)
200
300
400
500
600
700
800
900
1000
Temperature (°C)
0
1
2
3
4
5
6
7
8
Mole fraction V (%)
β
β + α
α
no O

## Slide 8: Ti-V + O
calculated using
current model
α region
β region
α + β region
phase boundary
Experiments
Solubility ( ) measured on ultra-high purity materials
Molokanov et al. (1977)
200
300
400
500
600
700
800
900
1000
Temperature (°C)
0
1
2
3
4
5
6
7
8
Mole fraction V (%)
β
β + α
α
no O
0.5 wt% O
Addition of O decreases the solubility of V in α-Ti…
…and increases the β–transus temperature

## Slide 9: Ti-6Al-4V + O
0
0.1
0.2
0.3
0.4
0.5
0.6
0.7
0.8
0.9
1.0
Phase fraction
200
400
600
800
1000
Temperature (°C)
β
α
Ti 6-4 (only Ti-Al-V)
Temperature (°C)
200
400
600
800
1000
1200
β
α
Ti3Al
+ 1 wt%O
200
400
600
800
1000
1200
β
α
Ti3Al
Temperature (°C)
+ 0.2 wt%O
Addition of O increase the β-transus temperature…
…and stabilizes the Ti3Al

## Slide 10: Al-V-Ti Diffusion in the Literature
β (bcc)
Li et al. (2002)
Ghosh et al. (2002)
Q. Chen (2004) (unpublished)
Wang et al. (2010) (no parameters)
Huang et al. (2010)
Y. Chen (2014)
J. Tran (2009)
α (hcp)
Q. Chen (2004) (unpublished)
J. Tran (2009)
Calphad Mobility Assessments
Diffusion Coefficients
Measured self- and impurity diffusion coefficients
Al impurity diffusion in α and β-Ti
V impurity diffusion in β-Ti
Ti self-diffusion in α and β-Ti
Measured interdiffusion coefficients
Al-Ti, V-Ti and Al-V-Ti for the β phase
Al-Ti for the α phase
Calculated from first-principles
Ti self-diffusion in α-Ti
Al and V impurity diffusion in α-Ti

## Slide 11: Diffusion Couple Experiments
  Seven diffusion paths at each temperature
  Impurity diffusion coefficients of Al and V in Ti
  Binary interdiffusion coefficients Al-Ti and V-Ti
  Ternary diffusion coefficients at three compositions
Isothermal section Ti-Al-V, 750°C
2
4
6
8
10
12
14
16
18
0
1
2
3
4
5
6
Mole fraction Al (%)
Mole fraction V (%)
A
B
C
E
D

α + β
α
α + Ti3Al





## Slide 12: Diffusion Couple Experiments
Isothermal section Ti-Al-V, 750°C
2
4
6
8
10
12
14
16
18
0
1
2
3
4
5
6
Mole fraction Al (%)
Mole fraction V (%)
A
B
C
E
D

α + β
α
α + Ti3Al




  Selection of end-member compositions
  Arc-melting, homogenization
  Heat treatment for interdiffusion
    650 °C: 2400 h
    750 °C: 150 h
    850 °C: 600 h
  Measure concentration profiles at contacts
    EDS/WDS

## Slide 13: Ti-V
2
4
6
8
10
12
14
16
18
0
1
2
3
4
5
6
Mole fraction Al (%)
α + β
α
α + Ti3Al
Mole fraction V (%)
A
B
C
E
D





Chart: Distance, µm
750 °C
Mole fraction V
Chart: Distance, µm
650 °C
Mole fraction V
Chart: 
Mole Fraction Vanadium
Interdiffusion coefficient m2/s
Sauer-Fries
Forward-simulation
650 °C
750 °C
Impurity diffusion coefficient:
Intermetallics 34 (2013)/J. Alloys Comp. 604 (2014)
Courtesy Zhangqi Chen , Ohio State
A: Ti
B: Ti-V
A: Ti
B: Ti-V

## Slide 14: Ti-Al
Chart: Mole Fraction Al (%)
Chart: Distance, µm
Chart: Distance, µm
2
4
6
8
10
12
14
16
18
0
1
2
3
4
5
6
Mole fraction Al (%)
α + β
α
α + Ti3Al
Mole fraction V (%)
A
B
C
E
D





A: Ti
D: Ti-Al
Mole fraction Al
750 °C
A: Ti
D: Ti-Al
Mole fraction Al
Interdiffusion coefficient m2/s
Sauer-Fries
Forward-simulation
850 °C
Impurity diffusion coefficient:
Intermetallics 34 (2013)/J. Alloys Comp. 604 (2014)
Courtesy Zhangqi Chen , Ohio State
850 °C

## Slide 15: Ti-Al-V
Chart: 
distance/√t (m·s-1/2)
Mole Fraction Vanadium
2
4
6
8
10
12
14
16
18
0
1
2
3
4
5
6
Mole fraction Al (%)
α + β
α
α + Ti3Al
Mole fraction V (%)
A
B
C
E
D





Concentration profile for V
A: Ti
B: Ti-V

## Slide 16: Ti-Al-V
Chart: 
distance/√t (m·s-1/2)
Mole Fraction Vanadium
2
4
6
8
10
12
14
16
18
0
1
2
3
4
5
6
Mole fraction Al (%)
α + β
α
α + Ti3Al
Mole fraction V (%)
A
B
C
E
D





Concentration profile for V
A: Ti
B: Ti-V
E: Ti-6Al

## Slide 17: Ti-Al-V
Observed trend: V diffusion in α-Ti decreases with increasing Al
Concentration profile for V
Chart: 
A: Ti
B: Ti-V
E: Ti-6Al
D: Ti-12Al
Distance/√t (m·s-1/2)
Mole Fraction Vanadium
2
4
6
8
10
12
14
16
18
0
1
2
3
4
5
6
Mole fraction Al (%)
α + β
α
α + Ti3Al
Mole fraction V (%)
A
B
C
E
D





Impurities?
≈ 500 ppm O, ≈ 200 ppm Fe
Different alloys – different conditions at contacts?
X-ray photoelectron spectroscopy

## Slide 18: X-ray Photoelectron Spectroscopy
oxide
O in alloy
Oxygen (%)
  Oxide layer thickness
    ≈ 3.5 - 4 nm
  Oxygen depth profile
    ≈ 5 - 8 nm (very uncertain!)
A: Ti
B: Ti-V
E: Ti-6Al
D: Ti-12Al
Oxide layer thickness (nm)
Oxide layer thickness (nm)
Oxide layer thickness
Work by Justin Gorham, NIST

## Slide 19: CALPHAD Diffusion Mobility Modeling
Intrinsic diffusion coefficient
(lattice-fixed frame of reference)
n … dependent species
Tracer diffusion coefficient
Interdiffusion coefficient
(volume-fixed frame of reference)
Stored in CALPHAD mobility databases as and
‘end-members’
interactions
Atomic Mobility
‘end-members’
k … diffusing species
j … gradient species

## Slide 20: CALPHAD Diffusion Mobility Modeling
parameter for Al mobility in α-Ti
from experiments
parameter for Ti mobility in α-Ti
from experiments
parameter for V mobility in α-Ti
from experiments
parameter for Al mobility in α-Al
parameter for V mobility in α-V
parameter for V mobility in α-Al

## Slide 21: Diffusion Coefficient Data
-22
-21
-20
-19
-18
-17
-16
-15
Logarithm of α-Ti self-diffusion
8.0
8.5
9.0
9.5
10.0
10.5
11.0
11.5
12.0
104·T-1 (K-1)
α-Ti self-diffusion coefficient
Herzig et al. (1991): c-axis
T
Koppers et al. (1997): c-axis (ultrapure)
T
Koppers et al. (1997): c-axis (ultrapure)
II
Koppers et al. (1997): c-axis
T
Xu et al. (2016): DFT c-axis
II
Xu et al. (2016): DFT c-axis
T
Shang et al. (2016): DFT c-axis
II
Shang et al. (2016): DFT c-axis
T

## Slide 22: Diffusion Coefficient Data
-22
-21
-20
-19
-18
-17
-16
-15
Logarithm of α-Ti self-diffusion
8.0
8.5
9.0
9.5
10.0
10.5
11.0
11.5
12.0
104·T-1 (K-1)
α-Ti self-diffusion coefficient
Herzig et al. (1991): c-axis
T
Koppers et al. (1997): c-axis (ultrapure)
T
Koppers et al. (1997): c-axis (ultrapure)
II
Koppers et al. (1997): c-axis
T
Xu et al. (2016): DFT c-axis
II
Xu et al. (2016): DFT c-axis
T
Shang et al. (2016): DFT c-axis
II
Shang et al. (2016): DFT c-axis
T
≈ 40 ppm Fe + Ni
ultrapure Ti

## Slide 23: Diffusion Coefficient Data
Raisanen (1985)
Koppers et al. (1997): c-axis (ultrapure)
T
Koppers et al. (1997): c-axis (ultrapure)
II
Koppers et al. (1997): c-axis
T
Koppers et al. (1997): c-axis
II
Araujo & Behar (2000)
Xu et al. (2016): DFT c-axis
II
Xu et al. (2016): DFT c-axis
T
-22
-21
-20
-19
-18
-17
-16
-15
Logarithm of Al impurity diffusion in α-Ti
8.0
8.5
9.0
9.5
10.0
10.5
11.0
11.5
12.0
Al diffusion coefficient in α-Ti
104·T-1 (K-1)
This work

## Slide 24: Diffusion Coefficient Data
Raisanen (1985)
Koppers et al. (1997): c-axis (ultrapure)
T
Koppers et al. (1997): c-axis (ultrapure)
II
Koppers et al. (1997): c-axis
T
Koppers et al. (1997): c-axis
II
Araujo & Behar (2000)
Xu et al. (2016): DFT c-axis
II
Xu et al. (2016): DFT c-axis
T
Al diffusion coefficient in α-Ti
>1000 ppm impurities
This work
-22
-21
-20
-19
-18
-17
-16
-15
Logarithm of Al impurity diffusion in α-Ti
8.0
8.5
9.0
9.5
10.0
10.5
11.0
11.5
12.0
104·T-1 (K-1)
>700 ppm impurities
≈ 1000 ppm impurities
ultrapure Ti

## Slide 25: Diffusion Coefficient Data
Xu et al. (2016): DFT c-axis
II
Xu et al. (2016): DFT c-axis
T
V diffusion coefficient in α-Ti
This work: ≥ 700 ppm impurities
-22
-21
-20
-19
-18
-17
-16
-15
-14
-13
-12
8.0
8.5
9.0
9.5
10.0
10.5
11.0
11.5
12.0
Logarithm of V impurity diffusion in α-Ti
104·T-1 (K-1)

## Slide 26: CALPHAD Diffusion Mobility Modeling
parameter for Al mobility in α-Ti
from experiments
parameter for Ti mobility in α-Ti
from experiments
parameter for V mobility in α-Ti
from experiments
Xin et al.: Met. Mat. Trans. A (2016)
empirical relationship
parameter for V mobility in α-Al
J. Askill: IFI/Plenum Publishing Corporation (1970)
empirical relationship
parameter for Al mobility in α-Al
parameter for V mobility in α-V
empirical relationship

## Slide 27: Diffusion Mobility Modeling
Chart: 
850 °C
A: Ti
D: Ti-12Al
distance/√t (m·s-1/2)
Mole Fraction Aluminum
750 °C
distance/√t (m·s-1/2)
Mole Fraction Aluminum
Chart: 
A: Ti
D: Ti-12Al

2
4
6
8
10
12
14
16
18
0
1
2
3
4
5
6
Mole fraction Al (%)
α + β
α
α + Ti3Al
Mole fraction V (%)
A
B
C
E
D





DICTRA calculations
Experiment

## Slide 28: Diffusion Mobility Modeling
Chart: 
Chart: 
650 °C
750 °C
A: Ti
A: Ti
B: Ti-V
B: Ti-V
distance/√t (m·s-1/2)
distance/√t (m·s-1/2)
Mole Fraction Vanadium
Mole Fraction Vanadium
2
4
6
8
10
12
14
16
18
0
1
2
3
4
5
6
Mole fraction Al (%)
α + β
α
α + Ti3Al
Mole fraction V (%)
A
B
C
E
D





DICTRA calculations
Experiment

## Slide 29: Diffusion Mobility Modeling
Chart: 
Chart: 
E: Ti-6Al
E: Ti-6Al
distance/√t (m·s-1/2)
distance/√t (m·s-1/2)
Mole Fraction Vanadium
Mole Fraction Vanadium
2
4
6
8
10
12
14
16
18
0
1
2
3
4
5
6
Mole fraction Al (%)
α + β
α
α + Ti3Al
Mole fraction V (%)
A
B
C
E
D





A: Ti
A: Ti
B: Ti-V
B: Ti-V
650 °C
750 °C
DICTRA calculations
Experiment

## Slide 30: Diffusion Mobility Modeling
Chart: 
Chart: 
D: Ti-12Al
D: Ti-12Al
distance/√t (m·s-1/2)
distance/√t (m·s-1/2)
Mole Fraction Vanadium
Mole Fraction Vanadium
2
4
6
8
10
12
14
16
18
0
1
2
3
4
5
6
Mole fraction Al (%)
α + β
α
α + Ti3Al
Mole fraction V (%)
A
B
C
E
D





E: Ti-6Al
E: Ti-6Al
A: Ti
A: Ti
B: Ti-V
B: Ti-V
650 °C
750 °C
DICTRA calculations
Experiment

## Slide 31: Summary
The developed thermodynamic CALPHAD model accounts for the effect of oxygen on the Ti-Al-V system
  Oxygen effects phase fractions
  Increases the β-transus temperature
  Stabilizes Ti3Al at lower Al contents and at higher temperatures
Diffusion couple experiments
  The presence of Al in the α-Ti matrix slows down the diffusion of V
Diffusion mobility modeling
  Preliminary mobility modeling accounts for the compositional effect of Al

## Slide 32: Future Work
Left to do…
  Complete analyses of diffusion couple experimental results
  Complete diffusion mobility modeling
Future challenge
  How to treat impurity-enhanced diffusion in Ti?
-22
-21
-20
-19
-18
-17
-16
-15
Logarithm of Al impurity diffusion in α-Ti
8.0
8.5
9.0
9.5
10.0
10.5
11.0
11.5
12.0
104·T-1 (K-1)
>1000 ppm
≈ 1000 ppm impurities
ultrapure Ti
> 700 ppm
Al diffusion coefficient in α-Ti

## Slide 33
Thank you!