## Slide 1: Magnetic Phase Transition and Spin Wave Excitations in the Colossal Magnetoresistive Manganites: La1−xSrxMnO3 (x = 0.3)
Rebecca Dally, Yang Zhao, William Ratcliff, Jeffrey Lynn
29th CHRNS School on Methods and Applications of Neutron Spectroscopy
July 17-21, 2023

## Slide 2: Outline
Magnetic structures and excitations
  Static: Magnetic structures
  Dynamic: Spin Waves
  Ideal isotropic ferromagnet
Example: Fe3Sn2
Example: La1−xSrxMnO3
  Colossal Magnetoresistance
  Paramagnetic Insulator <-> Ferromagnetic Metal
Spin-Wave calculation (SpinW)
  MATLAB package
Polarized inelastic neutron scattering: α-NaMnO2

## Slide 3: Magnetic Structures:
magnetic structures: allowed magnetic Bragg peak locations coincide with allowed positions from nuclear structure
V. O. Garlea and B. C. Chakoumakos, "Magnetic Structures" in Experimental Methods in the Physical Sciences, ed. F. Fernandez-Alonso and D. L. Price (Academic Press, 2015). https://doi.org/10.1016/B978-0-12-802049-4.00004-X

## Slide 4: Magnetic Structures: , commensurate
In order to describe the magnetic structure with respect to the nuclear structure, you may need more than one unit cell
V. O. Garlea and B. C. Chakoumakos, "Magnetic Structures" in Experimental Methods in the Physical Sciences, ed. F. Fernandez-Alonso and D. L. Price (Academic Press, 2015). https://doi.org/10.1016/B978-0-12-802049-4.00004-X

## Slide 5: Magnetic Structures: incommensurate
V. O. Garlea and B. C. Chakoumakos, "Magnetic Structures" in Experimental Methods in the Physical Sciences, ed. F. Fernandez-Alonso and D. L. Price (Academic Press, 2015). https://doi.org/10.1016/B978-0-12-802049-4.00004-X

## Slide 6: Magnetic Structures: multi-k (e.g. skyrmions)
Wang, S., Tang, J., Wang, W. et al. Electrical Detection of Magnetic Skyrmions. J Low Temp Phys 197, 321–336 (2019). https://doi.org/10.1007/s10909-019-02202-w
Tokunaga, Y. et al. A new class of chiral materials hosting magnetic skyrmions beyond room temperature. Nat. Commun. 6:7638 doi: 10.1038/ncomms8638 (2015).

## Slide 7: Magnetic excitations
Magnons (quantized spin waves) are (bosons) quasiparticles
Neutrons can only detect events
  Note: neutron studies on spinons ( bosons) are detecting two-spinon interactions
ground state
(static magnetic structure)
excited state
elastic
(neutron diffraction)
inelastic neutron scattering (INS)

## Slide 8: Ideal NN isotropic Heisenberg ferromagnet
,
, , and components of spins interact equally with exchange coupling strength,
Ground state energy:
Dispersion relation:
z = # NNs
(6 for cubic)
N = # unit cells

## Slide 9: Ideal NN isotropic Heisenberg ferromagnet
,
, , and components of spins interact equally with exchange coupling strength,
Ground state energy:
Excited state:

## Slide 10: Ideal NN isotropic Heisenberg ferromagnet
  Note: antiferromagnet linear in near
Reality:
  could be actual field, dipolar interactions, very small anisotropy

## Slide 11: Magnetic excitations: Fe3Sn2
R. L. Dally, et al. Isotropic nature of the metallic kagome ferromagnet Fe3Sn2 at high temperatures. Crystals, 11, 307 (2021). https://doi.org/10.3390/cryst11030307

## Slide 12: Magnetic excitations: Fe3Sn2
INS on powder samples  get Q-integrated data
Near Q = 0, only integrating about a single zone center
H
K
Q
B. Yuan, et al. Phys. Rev. B 98, 214433 (2018).

## Slide 13: Magnetic excitations: Fe3Sn2
R. L. Dally, et al. Isotropic nature of the metallic kagome ferromagnet Fe3Sn2 at high temperatures. Crystals, 11, 307 (2021). https://doi.org/10.3390/cryst11030307

## Slide 14: Magnetic excitations: Fe3Sn2
R. L. Dally, et al. Isotropic nature of the metallic kagome ferromagnet Fe3Sn2 at high temperatures. Crystals, 11, 307 (2021). https://doi.org/10.3390/cryst11030307
Typical for 3D Heisenberg exchange FM

## Slide 15: La1−xSrxMnO3 basics
LaMnO3
Ideal Perovskite Structure (Pseudo-Cubic)
Colossal Magnetoresitive
Colossal >> Giant (GMR HD heads)

## Slide 16: La1−xSrxMnO3 Phase Diagram
F, P, CN, M, I
ferromagnetic, paramagnetic, spin-canted antiferromagnetic, metallic, insulating
A. Urushibara, et al. Phys. Rev. B 51, 14103 (1995). https://doi.org/10.1103/PhysRevB.51.14103

## Slide 17
La1−xSrxMnO3 Phase Diagram
F, P, CN, M, I
ferromagnetic, paramagnetic, spin-canted antiferromagnetic, metallic, insulating
A. Urushibara, et al. Phys. Rev. B 51, 14103 (1995). https://doi.org/10.1103/PhysRevB.51.14103

## Slide 18
Doping Sr2+ for La3+: Mn3+  Mn4+
Antiferromagnetic  Ferromagnetic (spins)
Insulating  Metallic (hole doping)
La1−xSrxMnO3 Phase Diagram
F, P, CN, M, I
ferromagnetic, paramagnetic, spin-canted antiferromagnetic, metallic, insulating
A. Urushibara, et al. Phys. Rev. B 51, 14103 (1995). https://doi.org/10.1103/PhysRevB.51.14103

## Slide 19: Coupling between degrees of freedom
Spins
Lattice
Electron

## Slide 20: Basic Interactions (Double exchange)
d
eg
t2g
Strong Hund’s Rule Coupling
(on-site electrons must be parallel)
Mn3+ in LaMnO3

## Slide 21: Basic Interactions (Continue)
eg electron can only hop if core spins are parallel with nearby empty site
Jahn-Teller Distortion couples spins with lattice, i.e. Ferromagnetic coupling
Mn3+
Mn4+

## Slide 22: Ferromagnetic Long-Range Ordering
T (K)
TC = 336.3(5) K
Q = (1, 0, 0)
Bragg Peak: Magnetic + Structural

## Slide 23: Spin Wave Excitations
L. Vasiliu-Doloc, et al. Phys. Rev. B 58, 14913 (1998). https://doi.org/10.1103/PhysRevB.58.14913

## Slide 24: What is SpinW?
Open source MATLAB package
Developed at HBZ/PSI
Numerically solves eigenvalue/vectors of spin Hamiltonians using linear spin-wave theory:
Uses Rotating reference frame – can do incommensurate structures.
Lots of tools contained within! (energy minimization, diffuse scattering, fitting, etc.)

## Slide 25: Spin Wave Excitations and Polarized Neutrons: α-NaMnO2
R. L. Dally, et al. Amplitude mode in the planar triangular antiferromagnet Na0.9MnO2. Nat Commun 9, 2188 (2018). https://doi.org/10.1038/s41467-018-04601-1
all spins || [-1,0,1]
quasi-1D excitations

## Slide 26: Spin Wave Excitations and Polarized Neutrons: α-NaMnO2
R. L. Dally, et al. Amplitude mode in the planar triangular antiferromagnet Na0.9MnO2. Nat Commun 9, 2188 (2018). https://doi.org/10.1038/s41467-018-04601-1

## Slide 27: Spin Wave Excitations and Polarized Neutrons: α-NaMnO2
R. L. Dally, et al. Amplitude mode in the planar triangular antiferromagnet Na0.9MnO2. Nat Commun 9, 2188 (2018). https://doi.org/10.1038/s41467-018-04601-1

## Slide 28: Outline
Magnetic structures and excitations
  Static: Magnetic structures
  Dynamic: Spin Waves
  Ideal isotropic ferromagnet
Example: Fe3Sn2
Example: La1−xSrxMnO3
  Colossal Magnetoresistance
  Paramagnetic Insulator <-> Ferromagnetic Metal
Spin-Wave calculation (SpinW)
  MATLAB package
Polarized inelastic neutron scattering: α-NaMnO2