## Slide 1
Introduction to Polarized Neutron Reflectometry

## Slide 2
What Will We Learn Today
What samples are ideal for PNR?
What information does PNR provide?
What does PNR data look like?
How do we understand PNR data?
How do I design a PNR experiment?
and finally… what does PNR stand for?
Polarized Neutron Reflectometry

## Slide 3
Neutron Reflectometers at the NCNR
CANDOR
NG7 REFL
PBR
MAGIK
The NCNR currently operates 4 neutron reflectometers, three of which can run polarized measurements

## Slide 4
Depth Profiling Thin Stuff
Scanning Transmission Electron Microscopy
Rutherford Backscattering
V. I. Bachurin et al., (2019) https://doi.org/10.1134/S102745101902023X
X-ray Reflectivity
Secondary Ion Mass Spectrometry
There are a lot of ways to depth profile thin flms, so why do it with neutrons?
Neutrons are very good at some very specific things

## Slide 5
X-Rays
Neutrons
C
Fe
C
Fe
H
D
Interacts through Strong Force
(Actually Negative!)
Light element sensitivity!
No charge
Voltage bias or Current Flow
C. H. Lee et al., Journal of Power Sources 412, 725 (2019)
What are Neutrons Really Good At?
Biology – Protein Binding and Lipid Bilayers
D. P. Hoogerheide et al., Biochimica et Biophysica Acta (BBA) – Biomembranes, 1863, 186343 (2021)
Notes: X-ray cross section related to electron density (Z), complicated sample environment + D/H sensitivity enables unique bio experiments

## Slide 6
Neutron Reflectometry (NR)
n0
n0
n0
detector
U235 reactor
Neutron Reflectometry
Thin films
1 nm – 300 nm thick
Samples must be shiny!
Brian Maranville’s Reflectivity Simulator
https://www.ncnr.nist.gov/instruments/magik/d3-science-v4/demos/reflectometer_alignment_sim_three.html
https://www.nist.gov/ncnr/magik-reflectometer  Alignment Simulator

## Slide 7
n0
detector
U235 reactor
Neutron Reflectometry
Slower Neutrons
1 nm – 300 nm structures
Thin Films
Samples must be shiny!
=
- is the scattering vector
Elastic scattering implies:
2θ
Incident wave vector with
θ
Neutron Reflectometry (NR)

## Slide 8
Angle
Roughness
I ~ 1/Q4
Thickness
Density/Contrast
n0
detector
U235 reactor
Neutron Reflectometry
Slower Neutrons
1 nm – 300 nm structures
Thin Films
Samples must be shiny!
6-8 orders of magnitude
Neutron Reflectometry (NR)

## Slide 9
Interpreting NR Data: Fitting
We can explicitly solve the 1D Schrödinger equation for a slab or series of slabs
C. F. Majkrzak, K. V. O’Donovan, N. F. Berk
Change Model
Data
Model
Compare
Calculate Reflectometry
Refl1D Software Package:
https://www.nist.gov/ncnr/data-reduction-analysis/reflectometry-software

## Slide 10
NR Output: SLD Profiles
Scattering Length Density Profile:
D2O
CM4
H2O

## Slide 11
NR Output: SLD Profiles
D2O
CM4
H2O
Each slab has a:
Nuclear SLD
  Complex Number
  Imaginary part is absorption
Thickness
Roughness
  “Gaussian” roughness
  This usually applies

## Slide 12
Spin ½ particle interacts with magnetic fields
Ideal for magnetic characterization
n
The Magnetic Neutron
Fitzsimmons and Majkrzak: https://www.ncnr.nist.gov/instruments/pbr/references/Fitz.pdf

## Slide 13
n
Scattering!
n
Polarization Analysis:
Spin ½
Interacts with Magnetic Fields
Neutron Spin and Polarization Analysis
Spin Up
Spin Up
Non-spin flip

## Slide 14
Polarization Analysis:
Spin ½
Interacts with Magnetic Fields
n
Scattering!
n
Neutron Spin and Polarization Analysis
Spin Dn
Spin Dn
Non-spin flip

## Slide 15
Polarization Analysis:
Spin ½
Interacts with Magnetic Fields
n
Scattering!
n
Neutron Spin and Polarization Analysis
Spin Up
Spin Dn
Spin flip

## Slide 16
Polarization Analysis:
Spin ½
Interacts with Magnetic Fields
n
Scattering!
n
Neutron Spin and Polarization Analysis
Spin Dn
Spin Up
Spin flip

## Slide 17
4.75 Å Neutrons!
Polarized Beam Reflectometer
Q

## Slide 18
Non-spin flip (↑↑ or ↓↓)
  M ∥ H
  SLD↑↑ = ρN(Z) + ρM∥(Z)
  SLD↓↓ = ρN(Z) – ρM∥(Z)
  ρN =
  ρM =
  M = ρM/(2.853×10-9 Å-2 cm3/emu)
Q
↑↑
Polarization
↑↑
↓↑
✓
↑↓
✓
M
M
M
X
Scattering Cross Section Sensitivity
Notes: The total SLD has contributions from M and N

## Slide 19
Non-spin flip (↑↑ or ↓↓)
  M ∥ H
  SLD↑↑ = ρN(Z) + ρM∥(Z)
  SLD↓↓ = ρN(Z) – ρM∥(Z)
  ρN =
  ρM =
  M = ρM/(2.853×10-9 Å-2 cm3/emu)
Spin flip (↑↓ or ↓↑)
  M ⊥ H
  SLD↑↓ = ρM⟂(Z)
  SLD↓↑ = ρM⟂(Z)
Spin flip AND Non-spin flip
  M ⊥ Q
Q
↑↑
Polarization
↑↑
↓↑
✓
↑↓
✓
M
M
M
X
Scattering Cross Section Sensitivity
Notes: The SLD can be separated into nuclear and magnetic profiles

## Slide 20
SLD↑↑ = N(Z) + M(Z)
SLD↓↓ = N(Z) – M(Z)
R↑↑ = (N + M)2 = N2 + 2NM + M2
R↓↓ = (N - M)2 = N2 - 2NM + M2
Where N and M are the Fourier transform of the ρN and ρM profiles.
More complicated at the “Critical Edge”
SA = (↑↑ - ↓↓)/(↑↑ + ↓↓)= 2NM/(N+M)2
Polarized Neutron Reflectometry
Notes: Wavelike interaction spreads information about profile over all Q, so it needs to match at high Q as well as low Q

## Slide 21
SLD↑↑ = N(Z) + M(Z)
SLD↓↓ = N(Z) – M(Z)
Fresnel Reflectivity = R/Rsubstrate
Fresnel Difference = (↑↑ - ↓↓)/Rsubstrate
This approach makes it more obvious when your fits are bad
Polarized Neutron Reflectometry

## Slide 22
Scattering Length Density (SLD)
SLD↑↑ = N(Z) + M(Z)
SLD↓↓ = N(Z) – M(Z)
Fresnel Reflectivity = R/Rsubstrate
Fresnel Difference = (↑↑ - ↓↓)/Rsubstrate
Polarized Neutron Reflectometry

## Slide 23
Common Use Case: Magnetic Proximity
Electrical Transport
Magnetometry
Measures entire sample, reports aggregate properties
Probes conductive layers preferentially. Interpretation complex, not quantitative
What about a magnetic proximity effect?
Tm3Fe5O12
(Bi,Sb)2Se3
C. Tang et al., Science Advances 3, e1700307 (2017)

## Slide 24
Electrical Transport
Magnetometry
Measures entire sample, reports aggregate properties
Probes conductive layers preferentially. Interpretation complex, not quantitative
What about a magnetic proximity effect?
Tm3Fe5O12
(Bi,Sb)2Se3
C. Tang et al., Science Advances 3, e1700307 (2017)
Polarized Neutron Reflectometry
Magnetic X-ray Spectroscopy
Element-specific magnetic characterization
Depth-resolved magnetic characterization
Which layers are magnetic?
What direction are they pointing?
Dead layers? Proximity Effects? Interface coupling?
Common Use Case: Magnetic Proximity
Notes: This is a case where PNR is a tool well-suited to the job

## Slide 25
PNR provides extremely accurate depth profiles
  Structural
  Magnetic
Can ALSO extract parameters like density/composition
Sensitive enough to detect ~3% variations in oxygen content
Should We Trust PNR?

## Slide 26
A single unit cell of SrIrO3 with a net magnetization of 40 emu/cc
PNR Sensitivity

## Slide 27
SrRuO3 (1 u.c.)/SrTiO3 (3 u.c.)
PNR Sensitivity

## Slide 28
Here we see the simulated reflectivity of a 40 nm thick Ni film on MgO over a Q-range of 2 nm-1
PNR Case Studies
Highest SLD controls critical edge

## Slide 29
Here we see the simulated reflectivity of a 40 nm thick Ni film on MgO over a Q-range of 2 nm-1
PNR Case Studies
Highest SLD controls critical edge

## Slide 30
Same system, but 10 nm instead of 40 nm
PNR Case Studies
Why no offset critical edges?
Thickness!

## Slide 31
Same system, but 3 nm instead of 10 nm
PNR Case Studies

## Slide 32
Roughness Dependence

## Slide 33
Cr:(Bi,Sb)2Te3/GaAs
Lower SLD magnetic layer
Lower SLD magnetic layer

## Slide 34
Difficult (Real) Cases

## Slide 35
Contrast Matching

## Slide 36
Multiple Periodicities

## Slide 37
Information-rich superlattice peaks (Bragg reflections)
Negative scattering length density is a real thing
Superlattice

## Slide 38
Resolution Effects: Angle
High-Resolution
Low-Resolution
Δθ
Δθ

## Slide 39
Resolution Effects: Angle
High-Resolution
Low-Resolution
Δθ
Δθ

## Slide 40
Experiment Planning: Sensitivity
Talk to an instrument scientist
Think of a very specific question you want to answer
Think about what you expect various answers to your questions to look like and simulate
Optimize sample size and quality. Sharp interfaces, large areas!
Think about other profiles you might get. Is there model degeneracy?

## Slide 41
Experiment Planning: Model Degeneracy

## Slide 42
Experiment Planning: Model Degeneracy

## Slide 43
https://pages.nist.gov/reflectometry-calculators/magnetic-reflectivity-calculator.html
Experiment Planning: Simulation Tool

## Slide 44
Experiment Planning: Sample Size
5 cm
×
2 cm
Typical Maximum PNR Size
Typical Beam Size for 10×10 mm2 sample
1 mm
15 mm
Typical Beam Size for X-ray Reflectometer
0.1 mm
10 mm
Typical Beam Size for Synchrotron X-ray Source
0.1 mm
diameter
103 counts/sec
107 counts/sec
1013 counts/sec
(this number might be wrong but it’s so large it doesn’t matter)
Make a big, uniform sample

## Slide 45
CANDoR
Traditional continuous beam (reactor) reflectometers have a monochromator to select a single wavelength. CANDOR is a polychromatic reflectometer with massively increased data rates.
Experiment Planning: CANDOR Reflectometer

## Slide 46
CANDOR Q-range: Wavelength and Angle
λ from 4 Å – 6 Å
θ from 5.7° to 8.3°

## Slide 47
What I Hope You Learned
What samples are ideal for PNR
What information PNR provides
What PNR data looks like
How we understand PNR data
How to design a PNR experiment
and finally… what does PNR stand for?
Polarized Neutron Reflectometry

## Slide 48: Extra Slides

## Slide 49
Other Resolution Effects
Wavelength Uncertainty
Sample Curvature
Focusing
Defocusing

## Slide 50
ToF Q-range: Wavelength and Angle
λ from 4.5 Å – 10.5 Å (30 Hz)
λ from 4.5 Å – 7.5 Å (60 Hz)
ORNL SNS: MAGREF
Δθ

## Slide 51
ToF Q-range: Wavelength and Angle
λ from 2.1 Å – 12 Å
Δθ ≈ 0.06° vs 0° - 3° range
Q-range dominated by Δλ
RAL ISIS: POLREF
Δθ

## Slide 52: Polarized neutron reflectometry
PNR measures chemical and in-plane magnetization depth dependence
Tracking light elements
Non-trivial magnetization profiles
Penetrate through 100s of nm
Notes: Exchange springs, spirals, AF coupling, interfacial

## Slide 54
4.75 Å Neutrons!

## Slide 56
Neutron Reflectometry Data
Roughness
Thickness
Density/Contrast
n
Incident wave vector with
θ
=
- is the scattering vector
Elastic scattering implies:
2θ
Neutron reflectometry is sensitive to chemical and in-plane magnetization depth dependence

## Slide 57
Typical Beam Shapes and Sizes
5 cm
×
2 cm
Typical Maximum PNR Size
Typical Beam Size for 10×10 mm2 sample
1 mm
15 mm
Typical Beam Size for X-ray Reflectometer
0.1 mm
10 mm
Typical Beam Size for Synchrotron X-ray Source
0.1 mm
diameter
103 counts/sec
107 counts/sec
1013 counts/sec
(this number might be wrong but it’s so large it doesn’t matter)

## Slide 58
Footprint Correction

## Slide 59
Footprint Correction and Sample Shape

## Slide 60
Simulating Roughness vs. Steps

## Slide 61
Multiple Samples and Incoherent Sum

## Slide 62
Nevot-Croce vs. Full Optical Matrix

## Slide 63
NIST Center for Neutron Research