## Slide 1
Rebecca Dally
NIST Center for Neutron Research
rebecca.dally@nist.gov
Introduction to triple-axis spectrometers

## Slide 2
What do you do with diffraction and scattering of thermal or cold neutrons?
Neutron diffraction to solve crystal structures or magnetic structures; discern between nuclear and magnetic scattering (polarized neutrons)
Look for short-range and/or long-range order; study critical scattering
Inelastic neutron scattering probes excitations (e.g. phonons or magnons)
Study all of the above in variety of sample environments
  temperature
  pressure
  magnetic field
  electric field
  stress/strain

## Slide 3
neutron beam
collimator
monochromator
sample
analyzer
detector
1
2
2
2
2
3
5
6
4
Triple-axis spectrometer (TAS) basics: components
collimator
monochromator
BT-7

## Slide 4
neutron beam
collimator
monochromator
sample
analyzer
detector
1
2
2
2
2
3
5
6
4
Triple-axis spectrometer (TAS) basics: monochromator
Bragg’s Law
Variable incident energy
(14.7 meV)
Works for picking out detected energy using analyzer, too

## Slide 5
Triple-axis spectrometer (TAS) basics: samples
c||c*
a
b
a*
b*
crystal
YMn6Sn6
TAS studies usually study one 2D plane at a time: what do you want to study?

## Slide 6
Thinking in reciprocal space: hexagonal unit cell example
Real (direct) space
Reciprocal space
a
b
c*
c,
b*
a*
(0,1,0)
(0,0,0)
HK0 plane
nuclear Bragg peak
(1,0,0)

## Slide 7
Things in reciprocal space have meaning in real space!
Infinite repeating planes in real space are a point in reciprocal space.

## Slide 8
Things in reciprocal space have meaning in real space!
https://www.grandmetric.com/topic/4-waveforms-frequencies-bandwidth/

## Slide 9
Bragg’s Law, neutron diffraction, geometry, and the scattering vector
https://www.veqter.co.uk/residual-stress-measurement/x-ray-diffraction

## Slide 10
https://nmi3.eu/neutron-research/techniques-for-/dynamics/three-axis-spectroscopy.html
Triple-axis geometry
https://www.nist.gov/ncnr/bt-7-photos
Triple-axis spectrometer for diffraction experiments
Control Ei (equivalently , )
Control Ef (equivalently , )
Control sample orientation
scattering vector determined by instrument

## Slide 11
Bragg’s Law, neutron diffraction, geometry, and the scattering vector
https://www.veqter.co.uk/residual-stress-measurement/x-ray-diffraction

## Slide 12
Bragg’s Law, neutron diffraction, geometry, and the scattering vector
https://www.veqter.co.uk/residual-stress-measurement/x-ray-diffraction

## Slide 13
Thermal and cold neutrons for structural and magnetic studies
K  meV (Boltzmann constant)
https://universe-review.ca/I15-27-SPapp.png

## Slide 14
What is being measured in a neutron scattering experiment?
The double differential cross-section
Conservation of energy
Normalization to incident flux
Born approximation
Thermodynamic factor
http://www-llb.cea.fr/ecns2003/lectures/schober/ECNS2003_Schober_NeutronScattering.pdf

## Slide 15
Neutron-nuclear interaction and the scattering length
Interaction between neutron and nucleus is due to strong force – extremely short range
Scattering length – element specific
https://www.ncnr.nist.gov/resources/n-lengths/
Cross section,

## Slide 16
The scattering potential between the neutron and unpaired electrons
due to magnetic interaction between a neutron and a moving electron of momentum and spin
Magnetic moments
neutron:
electron:
https://cnx.org/contents/i1ZdCc7x@3/Orbital-Magnetic-Dipole-Moment-of-the-Electron
Due to electron orbital motion
Due to electron spin
https://byjus.com/physics/electron-spin/

## Slide 17
The scattering potential between the neutron and unpaired electrons
Neutron only “sees” component of which is perpendicular to
https://www.slideserve.com/may/neutron-and-x-ray-scattering-studies-of-spin-charge-and-orbital-order-in-tm-oxides
Can get directional information about magnetic moments
What are you really measuring?
  Fourier transform of the real space magnetization density

## Slide 18
Potentials in real and Fourier space
https://notes.dmaitre.phyip3.dur.ac.uk/npp/notes/Nuclear+Form+Factors.html
Potential coming from sample nuclei

## Slide 19
Potential distribution from magnetism much more complicated
https://notes.dmaitre.phyip3.dur.ac.uk/npp/notes/Nuclear+Form+Factors.html
Form factors:
https://www2.cpfs.mpg.de/~rotter/homepage_mcphase/manual/node137.html
https://link.springer.com/chapter/10.1007/978-3-319-92955-2_1

## Slide 20
Potentials in real and Fourier space
https://notes.dmaitre.phyip3.dur.ac.uk/npp/notes/Nuclear+Form+Factors.html
https://doi.org/10.1039/C5TC04041H
(7Li1−xFexOD)FeSe

## Slide 21
Reduce problem to sample-dependent structure factor
Let’s make things a lot simpler… (elastic scattering)
Scattering function or dynamic structure factor
Structure factor – easy to calculate!

## Slide 22
An example of what you can do with neutron diffraction: GaV4S8
Neutron diffraction to solve crystal structures or magnetic structures (…and study transitions of each, e.g. first or second order)

## Slide 23
An example of what you can do with neutron diffraction: GaV4S8
Neutron diffraction to solve crystal structures or magnetic structures (…and study transitions of each, e.g. first or second order)

## Slide 24
Y
Sn
Mn
How is a unit cell defined? What is the minimum repeating unit?
magnetic atoms only (Mn)
YMn6Sn6

## Slide 25
How is a unit cell defined? What is the minimum repeating unit?
TN ~ 340 K
paramagnetic to antiferromagnet at Néel temperature
strong ferromagnetic exchange coupling between in-plane Mn atoms
magnetic unit cell is doubled along the c-axis when compared to the nuclear unit cell

## Slide 26
The magnetic propagation vector in YMn6Sn6
https://doi.org/10.1103/PhysRevB.103.094413

## Slide 27
The magnetic propagation vector, (a.k.a. wave vector or )
https://www.sciencedirect.com/science/article/pii/B978012802049400004X

## Slide 28
Working with single crystals in diffraction

## Slide 29
Working with single crystals in diffraction: theta-2theta scans
(1,1,0)
(2,2,0)
(3,3,0)
Q
Q
(3,3,0)
(2,2,0)
(1,1,0)
H
K
(HK0) plane

## Slide 30
Working with single crystals in diffraction: theta-2theta scans
Q
Real (direct) space
Reciprocal space
a1
b1
b2*
a2*
a1*
b1*
a2
b2
(3,3,0)
(2,2,0)
(1,1,0)
H
K
(HK0) plane

## Slide 31
Working with single crystals in diffraction: theta-2theta scans
(3,3,0)
(2,2,0)
(1,1,0)
Q
H
K
(1,1,0)
(2,2,0)
(3,3,0)
Q
(HK0) plane

## Slide 32
Working with single crystals in diffraction: theta scans
(1,1,0)
(1,1,0)
Q
θ
θ
Theta scans (constant Q scans) give information on crystal quality (mosaic)

## Slide 33
Working with single crystals in diffraction: theta scans
constant Q lines
Real (direct) space
Reciprocal space
a1
b1
b1*
a1*
a2
b2
a2*
b2*

## Slide 34
Working with single crystals in diffraction: theta scans
constant Q lines
Real (direct) space
Reciprocal space
a1
b1
b1*
a1*
a2
b2
a2*
b2*

## Slide 35
Working with single crystals in diffraction: theta scans
Aluminum powder lines

## Slide 36
Working with single crystals in diffraction: resolution function
https://nmi3.eu/neutron-research/techniques-for-/dynamics/three-axis-spectroscopy.html
10.1016/j.softx.2016.06.002
Neutron beam not perfectly monochromatic + divergence along path

## Slide 37
Working with single crystals in diffraction: resolution function
(1,1,0)
(1,1,0)
Q
θ
θ

## Slide 38
Working with single crystals in diffraction: resolution function
(1,1,0)
(1,1,0)
Q
θ
θ

## Slide 39
Working with single crystals in diffraction: resolution function
(1,1,0)
(1,1,0)
Q
θ
θ

## Slide 40
Working with single crystals in diffraction: resolution function
(1,1,0)
(1,1,0)
Q
θ
θ

## Slide 41
Working with single crystals in diffraction: resolution function
(1,1,0)
(1,1,0)
Q
θ
θ

## Slide 42
Working with single crystals in diffraction: theta scans
constant Q lines
(1,1,0)
θ
Q
θ
θ

## Slide 43
Working with single crystals in diffraction: resolution function
Resolution-limited
  Can’t have peak narrower than resolution
Peaks broader than resolution give info about:
  Crystal quality
  Range or time scale information (short-range or short-lived gives Lorentzian shape)
  is in real space
(1,1,0)
θ

## Slide 44
Thank you for your attention!
Rebecca Dally
NIST Center for Neutron Research
rebecca.dally@nist.gov

## Slide 45
Thinking in reciprocal space: hexagonal unit cell example
crystal
c
a
b
Y
Sn
Mn

## Slide 46
Thinking in reciprocal space: hexagonal unit cell example
crystal
a
b
Y
Sn
Mn
c,

## Slide 47
Reciprocal space
Thinking in reciprocal space: hexagonal unit cell example
a
b
c,
Real (direct) space

## Slide 48
Thinking in reciprocal space: hexagonal unit cell example
Real (direct) space
Reciprocal space
a
b
c,

## Slide 49
Thinking in reciprocal space: hexagonal unit cell example
Reciprocal space
Miller indices are in reciprocal lattice units (r.l.u.), such that:
()
()
()
Units are (momentum)

## Slide 50
Thinking in reciprocal space: hexagonal unit cell example
Real (direct) space
Reciprocal space
a
b
c*
c,
b*
a*
(0,1,0)
(0,0,0)
HK0 plane
nuclear Bragg peak
(1,0,0)

## Slide 51
Thinking in reciprocal space: hexagonal unit cell example
Real (direct) space
Reciprocal space
a
b
c*
c,
b*
a*
(1,0,0)
(0,1,0)
(1,1,0)
(2,0,0)
(0,2,0)
(2,2,0)
(2,1,0)
(1,2,0)
(-1,1,0)
(-1,2,0)
(0,0,0)
(2,-1,0)
(1,-1,0)
(0,-1,0)
(-1,-1,0)
(-1,0,0)
HK0 plane
nuclear Bragg peak

## Slide 52
Thinking in reciprocal space: hexagonal unit cell example
Real (direct) space
Reciprocal space
c*,c,
-a*b*,
-ab,
a*b*
ab
(1,1,0)
(2,2,0)
(0,0,0)
(-1,-1,0)
HHL plane
nuclear Bragg peak
(1,1,1)
(1,1,2)
(1,1,-1)
(1,1,-2)
(0,0,1)

## Slide 53
Thinking in reciprocal space: magnetic structure in hexagonal unit cell
()
Real space magnetic unit cell
Recip. space magnetic cell
a
b
c,

## Slide 54
Thinking in reciprocal space: magnetic structure in hexagonal unit cell
Real (direct) space
Reciprocal space
c*,c,
-a*b*,
-ab,
a*b*
ab
(1,1,0)
HHL plane
nuclear Bragg peak
(0,0,1)
(0,0,0.5)
(1,1,0.5)
magnetic Bragg peak