## Slide 1: A POLARIZED BEAM CAN DO A LOT OF THINGS
Brian Kirby, NCNR

## Slide 2: READ THIS
C. Majkrzak, K. O'Donovan, and N. Berk, in Neutron Scattering from Magnetic Materials (Elsevier, 2006), pp. 397–471.

## Slide 3: WHAT SCATTERS NEUTRONS?
Not This!

## Slide 4: WHAT SCATTERS NEUTRONS?
Graphic courtesy Peter Gehring, NIST
nuclei:
magnetic fields:

## Slide 5: SCATTERING LENGTH DENSITY
Nuclear component

## Slide 6: SCATTERING LENGTH DENSITY
Magnetic component
ρM = |M| x 2.91 x 10-6 Å-2 cm3 emu-1 = |M| x 2.91 x 10-6 Å-2 kA-1 m
Just the magnetic field
B = µ0(M + H)
H usually doesn’t contribute to the contrast
Gaussian (emu/cc)
SI (kA/m)

## Slide 7: SCATTERING LENGTH DENSITY
M. R. Fitzsimmons and C. F. Majkrzak, in Modern Techniques for Characterizing Magnetic Materials, edited by Z. Zhu ( Kluwer, New York, 2005).
Nuclear & magnetic same order of magnitude!

## Slide 8: POLARIZED NEUTRON BEAMS
Control orientation of neutron moment with respect to magnetic moments being probed
Separate nuclear and magnetic contributions to the scattering
Provides vector magnetic information
Unpolarized beams are affected by magnetic features

## Slide 9: POLARIZED BEAM FOR A REFLECTOMETER

## Slide 10: POLARIZED BEAM FOR A REFLECTOMETER
NO ZEROS!!!

## Slide 11: POLARIZED BEAM FOR A REFLECTOMETER
C. Majkrzak, K. O'Donovan, and N. Berk, in Neutron Scattering from Magnetic Materials (Elsevier, 2006), pp. 397–471.

## Slide 12: POLARIZED BEAM FOR A REFLECTOMETER
C. Majkrzak, K. O'Donovan, and N. Berk, in Neutron Scattering from Magnetic Materials (Elsevier, 2006), pp. 397–471.
swissneutronics.ch

## Slide 13: POLARIZED BEAM FOR A REFLECTOMETER
Previous showed appropriate technology for a monochromatic reflectometer optimized for specular reflectivity, also be aware of:
Broadband polarizing cavities
3He polarizer / analyzer / flipper
RF flippers

## Slide 14: PNR SELECTION RULES
Consider 4 types of scattering from the sample
R--: Neutron moments antiparallel to H at sample, sample doesn’t flip neutrons
R++: Neutron moments parallel to H at sample, sample doesn’t flip neutrons
R-+: Neutron moments antiparallel to H at sample, sample flips neutrons
R+-: Neutron moments parallel to H at sample, sample doesn’t flip neutrons

## Slide 15: PNR SELECTION RULES
H
Z
^

## Slide 16: PNR SELECTION RULES
non spin-flip: in-plane M(z) || H
H
spin-flip: in-plane M(z) ⊥ H
reflectivity, R = |r|2
Z
^
Halperin Effect:
no magnetic scattering along Q
Model fit sld in terms of ρN , ρM , and φ

## Slide 17: PNR SELECTION RULES
Z
H
spin-flip: in-plane M(z)
reflectivity, R = |r|2
non spin-flip: just nuclear!
Halperin Effect:
no magnetic scattering along Q
^
Model fit sld in terms of ρN , ρM , and φ

## Slide 18: DEPTH PROFILE OF A COLINEAR MAGNET

## Slide 20: DEPTH PROFILE OF A NONCOLINEAR MAGNET

## Slide 22: DEPTH PROFILE OF EXPELLED FIELD IN A SUPERCONDUCTOR

## Slide 24: DEPTH PROFILE OF A NON-MAGNETIC SAMPLE WITH A MAGNETIC REFERENCE LAYER

## Slide 26: DEPTH PROFILE OF NUCLEAR POLARIZATION

## Slide 27
Nuclear scattering length is actually spin-dependent
For GaAs:
Similar to magnetic scattering

## Slide 28: SUMMARY
For specular reflectometry
Polarization is used to separate magnetic and nuclear contributions to the scattering
Simultaneously model-fit R for different polarization states to determine nuclear & magnetic depth profile
Selection rules of thumb:
  Non spin-flip, R++ & R--, give you the nuclear profile and the component of the net in-plane magnetization profile parallel to H (but, see below…)
  Spin-flip, R+- & R-+, give you the component of the net in-plane magnetization perpendicular to H
  Magnetic fields parallel to Q do not scatter neutrons – you can’t see perpendicular magnetic moments in films with specular PNR