## Slide 1
Choosing the Right Spectrometer
Guangyong Xu
NIST Center for Neutron Research
Thanks to Peter Gehring, Jeff Lynn, Dan Neumann, and Jim Ryhne for preparing many of the slides

## Slide 2
How do we “see”?
We see something when light scatters from it.
Light is composed of electromagnetic waves.
However, the details of what we see are ultimately limited by the wavelength.
Thus scattering conveys information!
l ~ 4000 A – 7000 A

## Slide 3
we require a probe with the wavelength l ~ length-scale of interest (angstroms, i.e. 10-10 m), as well as having the correct energy scale (meV).
Some candidates …
X-rays
Electrons
Neutrons
EM - wave
Neutral particle
Charged particle
How do we “see” atomic structures?

## Slide 4: Some Useful Formulas

## Slide 5
Let´s test the net ...
...the principle of scattering experiments
How do we study lattice structure/vibrations

## Slide 6: Conservation of Momentum and Energy

## Slide 7
Time space
w
2p/T
w-space
d
Real space
Q
2p/d
Q-space
~1/x
~1/G
T
time
Fs
Fs
x
G
Scattering measurements
Elastic scattering – static structures
Inelastic scattering – dynamics
Bragg peak
Diffuse scattering
Space-time (r,t)
Energy-momentum (Q, hw)
Fourier transformation

## Slide 8
Review: Main Messages of the Week
(1) Neutron scattering experiments measure the flux of neutrons scattered by a sample into a detector as a function of the change in neutron wave vector (Q) and energy (hw).
(2) The expressions for the scattered neutron flux F depend on the positions and motions of atomic nuclei or unpaired electron spins.
Energy
Momentum
hQ = hki - hkf
hw = hwi - hwf
hwn = h2kn2/2m
hkn = h(2p/ln)
F provides information about all of these quantities!
F = f{ri(t), rj(t), Si(t), Sj(t)}
F(Q,hw) =
neutrons
sec–cm2


## Slide 9
Neutron scattering is an intensity-limited technique where instrumental resolution and signal compete. Different instruments are optimized for different resolution and energy ranges.
Uncertainties in the neutron wavelength and direction imply Q and hw can only be defined with a finite precision.
Courtesy of R. Pynn
The total signal in a scattering experiment is proportional to the resolution volume  better resolution leads to lower count rates! Choose carefully …
Why So Many Different Spectrometers?

## Slide 10: Inelastic Spectrometers
High flux backscattering spectrometer (HFBS)
Disk chopper time-of-flight spectrometer (DCS) (FANS)
Spin-echo spectrometer (NSE)
Thermal triple-axis instruments (BT-7) (BT-4)
Cold neutron triple-axis instrument (MACS) (SPINS)
1 meV
250 eV
1 eV
t  ~50 neV
S(Q,E)
S(Q,t)
All these different spectrometers are designed differently to optimize intensity and resolution for different measurement requirements
Remember – Intensity
Resolution

## Slide 11
BT7, MACS, HFBS
1. Bragg Diffraction
nl=2dSinq
Crystal Spectrometers:
Specifying ki and kf
d
S(Q,E)
SPINS (Cold Triple Axis)
BT-4 (Thermal Triple Axis and Filter Analyzer Spectrometer)
BT-1 (High Resolution Powder Diffractometer)
BT-8 (Residual Stress Diffractometer)

## Slide 12
Triple-Axis Spectrometer (BT7, BT4, SPINS, MACS)
Monochromator
Sample
Analyzer
Detector
Neutron Source

## Slide 13: Reciprocal Space for Thermal Neutrons

## Slide 14
BT-7 Inelastic Scattering
Focusing Analyzer, PSD
Polarized Neutron Measurements
Journal of Research of NIST 117, 61-79 (2012)

## Slide 15: Magnetic Scattering from La(O,F)FeAs
PSD on
BT-7
C. de la Cruz, Q. Huang, J. W. Lynn, J. Li, W. Ratcliff II, J. L. Zarestky, H. A. Mook, G. F. Chen, J. L. Luo, N. L. Wang, and P. Dai,
Nature 453, 899 (2008).

## Slide 16: Polaron Dynamics in CMR La0.7Ca0.3MnO3
J. W. Lynn, D. N. Argyriou, Y. Ren, Y. Chen, Y. M. Mukovskii, and D. A. Shulyatev, Phys. Rev. B76, 014437 (2007)

## Slide 17: Energy Resolution for Crystal Spectrometers
E = C (2/)2
E = C´ / 3
Cold Neutrons higher resolution
Center for Neutron Research

## Slide 18: Reciprocal Space for Cold Neutrons
Q
MACS twenty points at a time; high flux horizontal focused monochromator
wide-angle polarization analysis capability

## Slide 19: Spin Liquid Scattering in ZnCu3(OD)6Cl2
Tian-Heng Han, Joel S. Helton, Shaoyan Chu, Daniel G. Nocera, Jose A. Rodriguez-Rivera, Collin Broholm,
and Young S. Lee, Nature 492, 406 (2012).
6 meV
2 meV
3/4 meV
T = 1.6 K
MACS
Notes: Inelastic neutron scattering from the spin excitations, plotted in reciprocal space. a–c, Measurements were made at T51.6K on a single crystal sample of ZnCu3(OD)6Cl2. The dynamic structure factor, Stot(Q,v), is plotted for Bv56meV (a) and Bv52meV (b) with Ef55.1 meV and Bv50.75 meV (c) with Ef53.0 meV. The background was measured ith an empty sample holder and subtracted. The diffuse scattering is mostly magnetic in origin, because the phonon contribution to the signal is small (except near the (2, 2, 0)-type positions, where the fundamental Bragg peaks are strong). d, The magnetic part of the dynamic structure factor, Smag(Q,v), integrated over 1#Bv#9meV. e, Calculation of the equal-time structure factor, Smag(Q), for a model of uncorrelated nearest-neighbour dimers. The intensity corresponds to 1/8 of the total moment sum rule S(S11) for the spins on the kagome lattice. The data presented in a–c are expressed in barn sr21 eV21 per formula unit, as shown by the left colour bars. The data presented in parts d and e are dimensionless, with the scale given by the right colour bar. The Brillouin zone boundaries are drawn in the figure for clarity; they correspond to the conventional unit cell with parameters a5b56.83A˚ , c514.05A˚ , a5b590u and c5120u.

## Slide 20: Perfect Resolution Backscattering
Thermal TA 1,000 eV
Cold TA 200 eV
HFBS 1 eV
Note: Scattering angle = 2

## Slide 21: Quantum Rotational Tunneling in Toluene: A Measurement using HFBS
Motion of methyl groups (CH3) in toluene (C6H5CH3)
Inelastic peaks correspond to tunneling through a potential barrier: a classically forbidden motion!
Tunneling rate ~6 GHz
Presence of two inelastic peaks on the energy loss side and two peaks on the energy gain side indicates two inequivalent sites for molecules in the solid
HFBS
E (eV)
Notes: Find out more about HFBS

## Slide 22
BT7, MACS, HFBS
1. Bragg Diffraction (Crystal Spectrometers)
2. Time-of-Flight (TOF)
DCS
nl=2dSinq
Methods of Specifying and Measuring ki and kf
d
L
v = L/t
S(Q,E)
S(Q,E)

## Slide 23: Disk Chopper Spectrometer
ki
kf
Q
Q
kf
Q
kf
Detector
913 Detectors

## Slide 24
Quantities varied
wavelength l
chopper slot widths W
I(E)
DE
Things to Consider When Choosing DCS
Remember – Intensity
Resolution

## Slide 25: Fractional Spin Excitations in Yb2Pt2Pb
L. S. Wu, W. J. Gannon, I. A. Zaliznyak, A. M. Tsvelik, M. Brockmann, J.-S. Caux, M. S. Kim, Y. Qiu, J. R. D. Copley, G. Ehlers, A. Podlesnyak, M. C. Aronson, Science 352, 1690 (2016).
Notes: Orbital-exchange and fractional quantum number excitations in an f-electron metal, Yb2Pt2Pb
Fractional spinon excitations in Yb2Pt2Pb. (A) The dispersion of the spectrum of magnetic excitations along the QL direction in reciprocal space of Yb2Pt2Pb at T = 0.1 K, obtained by averaging the scattered neutron intensity over the first Brillouin zone in QHH, along the perpendicular, ðH;H; 0Þ direction. Circles: onset of the excitation continuum determined by fitting the constant-QL data. Solid white lines: lower and upper boundaries of the two-spinon continua. Dashed lines: upper boundaries of the four spinon continua (6). (B) The dispersion of the scattered neutron intensity along the QHH direction for QL ¼ 0:5 T 0:1. (C) The partial static structure factor, MðQÞ, obtained by integrating the scattered intensity from 0.15 to 1.5 meV. MðQÞ depends on the relative orientation of the scattering vector Q ¼ ðH;H; LÞ and the direction of magnetic moment fluctuations (30). (D) At 4 T,MðQÞ (red squares) follows the projection of the (110) sublattice moments on the scattering wave vector (polarization factor Pð4 TÞ ¼ ðLcÞ2 2ðHaÞ2þðLcÞ2, red line), indicating that only magnetic fluctuations along the (110)moments contribute tomagnetic scattering. Both polarizations are present when B ¼ 0 T, consistent with equal longitudinal spinon spectral weight in both (110) and (1-10) sublattices. By subtracting the 4 Tdata from the 0 Tdata (black dots),we can isolate the scattering from fluctuations along the field direction, (1-10), which are always perpendicular to the scattering vector Q and whose polarization factor is constant (black line). The agreement between the polarization factors and our data confirms that only fluctuations of the Ybmoments that lie along the respective (110) or (1-10) direction are seen in our experiment and that there is no measurable transverse component of magnetic moment or excitations. Error bars in all figures represent 1 SD.

## Slide 26
Example: DCS versus BT7
Rules of Thumb: (think carefully before violating)
DCS, MACS – systems requiring resolution < 400 meV
BT7 – single crystals with specific points of interest
Limited regions in Q-w
BT7
Broad surveys in Q-w
DCS

## Slide 27
BT7, MACS, HFBS
1. Bragg Diffraction (Crystal Spectrometers)
2. Time-of-Flight (TOF)
DCS, HFBS
“TOF” Larmor Precession
NSE
nl=2dSinq
B
Methods of Specifying and Measuring ki and kf
d
L
v = L/t
S(Q,E)
S(Q,E)
S(Q,t)

## Slide 28: Spin Echo Spectrometer
Measures I(Q,t) instead of S(Q,ω)
Notes: Get more info

## Slide 29: Spin Echo Measurements on Polar Nano Regions in Relaxor Ferroelectric Systems
Zhijun Xu, Jinsheng Wen, Guangyong Xu, Chris Stock, Jason S Gardner, Peter M Gehring, Physical Review B, 82, 134124 (2010)
Notes: Use my own data

## Slide 30
The NCNR Menagerie of Instruments
Thermal Neutrons
Cold Neutrons

## Slide 31
How do I Choose the Right Spectrometer?
Two basic considerations:
2. What are the length scales (Q) of interest?
1. What are the time scales (E) of interest?
Two additional considerations:
2. What momentum resolution (DQ [or DQ]) is required?
1. What energy resolution (DE) is required?
(Some spectrometers overlap 
the choice may boil down to one of resolution)

## Slide 32
Different Spectrometers Cover Different Regions of Phase Space
Larger “objects” tend to exhibit slower motions.

## Slide 33
Rules of Thumb
hw > 1-100 meV - use a thermal triple-axis spectrometer like BT7.
1. What are the energies (hw), i.e. time scales (Dt ~1/w), of interest?
REMEMBER - Qmin and Qmax are inversely proportional to the
incident neutron wavelength
hw < 30 meV - use HFBS or NSE.
In between - use MACS or DCS or a cold-neutron triple-axis spectrometer like SPINS.
2. Make sure that the length scales L of the relevant motions lie within the range of the spectrometer. For example, consider the HFBS. (Q ~ 2p/L)
Qmin = 0.25 Å-1  Lmax~ 25 Å
Qmax = 1.75 Å-1  Lmin~ 3.5 Å

## Slide 34
Is your sample polycrystalline or amorphous?
Is the expected Q-dependence of the scattering weak?
YES? Consider instruments
with large analyzer areas.
More Rules of Thumb
NO? Consider using BT7, SPINS, or NSE.
MACS
DCS
HFBS
BT7
Does ONLY the magnitude (not the direction) of Q matter?
This often means that you want to look at a large region of Q-hw space,
or that you can sum the data over a large region of Q-hw space.

## Slide 35
Know as much about your sample as possible!!
(Beamtime costs ~ $5000/day!!)
General Sample “Design”
Magnetization vs T
Specific heat vs T
Muon spin relaxation
Raman spectroscopy
X-ray data
Other considerations:
What’s the structure (in a general sense)?
Are there any phase transitions (or a glass transition)?
What isotopes are present?
Supplementary data from other measurements …

## Slide 36
Try to avoid isotopes that are strongly absorbing.
6Li 10B 113Cd 157Gd
http://www.ncnr.nist.gov/resources/n-lengths
For a complete listing go to
General Sample “Design”
Almost all experiments of collective excitations involve coherent scattering
Avoid isotopes with strong incoherent scattering
If sample contains H it should be deuterated (D).

## Slide 37
Single crystals yield the most information.
Increase the intensity by increasing the amount of sample.
ki
kf
Almost all experiments of collective excitations involve coherent scattering
 If sample contains H it should be deuterated (D).
Sample “Design”
If you have a powder, use a cylindrical container (rather than flat plate).
Annular may be the best sample geometry.

## Slide 38
What ChatGPT says

## Slide 39
Organizers – Leland Harriger and Ryan Murphy
Administrative staff
Experiment teams
Invited speakers
Enjoy the Science!
Acknowledgements