## Slide 1: Looking at everything while looking at nothing an Introduction to Small-Angle Neutron Scattering
NIST Center for Neutron Research
Ryan P. Murphy

## Slide 2
Exposure 51
Credits: Photo of Rosalind Franklin courtesy of Vittorio Luzzati. Photo of x-ray crystallography
(Exposure 51) courtesy of King's College Archives. King's College London.
Rosalind Franklin
3.4 nm
0.34 nm
φ
DNA
φ

## Slide 3
“Seeing” collections of atoms
www.wichlab.com/research

## Slide 4
1016
How many particles are there?
NIST mAb
https://www.nist.gov/programs-projects/nist-monoclonal-antibody-reference-material-8671
≈ 10 nm
≈ 150 kg/mol
≈ 10 mg/mL
10,000,000,000,000,000

## Slide 5
106

## Slide 6
1010

## Slide 7
1013
Reynisfjara
Iceland

## Slide 8
https://www.flickr.com/photos/gsfc/
1013
Iceland
1016
Sand grains along coastlines on Earth

## Slide 9
How is it possible to measure the structure of so many things all at once?

## Slide 10
NG3
VSANS
NG7 SANS
NGB-10m SANS
NGB-30m SANS
BT5 USANS
Small-Angle
Neutron
Scattering
(SANS)

## Slide 11
What is scattering?
Why at small-angle?
Why use neutrons?

## Slide 12
What is scattering?
Why at small-angle?
Why use neutrons?

## Slide 13
Scattering
ki
source
sample
detector
transmitted
absorbed
scattered
ks

## Slide 16
Scattering

## Slide 17
Scattering

## Slide 18
q
space
real
space

## Slide 19
Fourier transform
Scattering intensity is related to the differences in scattering length density distribution, ρ(r)
Intensity ~ Fourier transform2 of ρ(r)

## Slide 20
adapted from Y. Liu
‘Colloidal interactions in solution’
( - )2
Contrast
‘neutron color’
Scattering space, q (Å-1)
~
q (Å-1)
=
Real space, r (Å)
x
q (Å-1)
x
Positions
‘interparticle’
‘between’
x
q (Å-1)
x
Shape
‘intraparticle’
‘inside’

## Slide 21
Demonstration
FFT Software:
Brian Maranville: https://ncnr.nist.gov/instruments/magik/calculators/fourier_webcam/
Brian Pauw: https://lookingatnothing.com/
Interaction
Orientation
Complex shapes
Phase loss
Contrast
Size
Shape
Distribution

## Slide 22
adapted from Y. Liu
‘Colloidal interactions in solution’
( - )2
Contrast
‘neutron color’
Scattering space, q (Å-1)
~
q (Å-1)
=
Real space, r (Å)
x
q (Å-1)
x
Positions
‘interparticle’
‘between’
x
q (Å-1)
x
Shape
‘intraparticle’
‘inside’

## Slide 23
scattering intensity
incoherent
scattering
coherent
scattering
particle volume fraction
scattering length density contrast
form
factor
structure
factor
background
*Useful primarily in simpler colloidal or nanoparticle systems

## Slide 24
What is scattering?
Why at small-angle?
Why use neutrons?

## Slide 25
“Seeing” collections of atoms
www.wichlab.com/research
Typical size from 1 nm to 10 µm

## Slide 26
Small-angle scattering
ki
transmitted
scattered
ks
q
I(q)
Bragg condition
1 nm to 10 µm
1 Å-1 to 0.00003 Å-1
30 to 0.0006

## Slide 27
USANS l = 2.4 Å, Dl/l = 6%, 0.0006  < q < 0.06 
vSANS-48m 4.5 < l < 20 Å, Dl/l=1% & 12.5%, 0.017  < q < 30 
NG7-30m 4.5 < l < 20 Å, 11% < Dl/l < 25%, 0.056  < q < 30 
NGB-30m 3.0 < l < 20 Å, 11% < Dl/l < 25%, 0.065  < q < 24 
nSOFT-10m 3.0 < l < 20 Å, 11% < Dl/l < 25%, 0.17  < q < 30 
D = 2π/q
6 µm 0.6 µm 600 Å 60 Å 6 Å
80 m

## Slide 28
NG3
VSANS
NG7 SANS
NGB-10m SANS
NGB-30m SANS
BT5 USANS

## Slide 29
sample
Wavelength
Hammouda, B. (2016). The SANS Toolbox. Gaithersburg, MD, NIST Center for Neutron Research.

## Slide 30
VSANS
Fractal dimensions
Cluster lengths
Second virial coefficients
Radius of gyration
Low-q
Particle radius
Radius distribution
Mid-q
Pore radius
Surface area
High-q

## Slide 31
What is scattering?
Why at small-angle?
Why use neutrons?

## Slide 32
Neutrons
Photons
Interact with nuclei
SLD differences
Isotope (H/D) variation
Magnetic structure
Non-destructive
Extreme environments
Lower flux
Fewer sources
Interact with electrons
Electron density differences
Ionizing damage (X-rays)
Finer q-resolution
Higher flux
Many sources

## Slide 33
Contrast
bi = scattering length
V = molecular volume
neutron
X-ray
scattering length*
*X-ray scale reduced by ~ 1.5X to compare with neutron scale
adapted from presentation by J. D. Copley
H
D
C
O
Al
Si
Fe
scattering length density calculator
https://www.ncnr.nist.gov/resources/activation/
Neutron image: Daniel Hussey/NIST

## Slide 34
Contrast variation
ρsolvent ≠ ρcore ≠ ρshell
core and shell are visible
ρsolvent = ρcore
shell is visible
ρsolvent = ρshell
core is visible

## Slide 35
Magnetic structures
Gilbert, D. A., et al. (2019). Physical Review Materials 3(1).

## Slide 36
Non-destructive
foams
biologicals
kinetics
Perticaroli, S., et al. (2020). Langmuir 36(48): 14763-14771.
Nguyen, M. H. L., et al. (2019). Biophys J 116(5): 755-759.
Yearley, E. J., et al. (2014). Biophys J 106(8): 1763-1770.

## Slide 37
Extreme environments
Shear rates ~ 10-3 to 107 s-1
Pressures ~ vacuum to 4400 bar
Temperatures ~ 1.5 K to 800 K
https://www.nist.gov/ncnr/sample-environment
Teixeira, S. C. M., et al. (2018).
Journal of Neutron Research 20(1-2): 13-23.

## Slide 38
Summary
What is scattering?
Why at small-angle?
Why use neutrons?
Intensity patterns due to a change in quantum particle momentum (angle), providing a q-space transform of scattering length density differences in real space
Probing length scales : 1 nm to 10 um
1 Å-1 to 0.00003 Å-1
30 to 0.0006
Unique element contrast, isotope variation, magnetic structure, non-destructive,
extreme and creative sample environments

## Slide 39
https://www.flickr.com/photos/gsfc/
1016
Sand grains along coastlines on Earth
Looking at everything
(in the beam path)

## Slide 40
Credits: Photo of Rosalind Franklin courtesy of Vittorio Luzzati. Photo of x-ray crystallography
(Exposure 51) courtesy of King's College Archives. King's College London.
Rosalind Franklin
3.4 nm
0.34 nm
φ
DNA
φ
Looking at nothing something?

## Slide 41
Rosalind Franklin Institute
Rutherford Appleton Laboratory
Didcot, Oxfordshire, UK

## Slide 42: Looking at everything while looking at something an Introduction to Small-Angle Neutron Scattering
NIST Center for Neutron Research
Ryan P. Murphy