## Slide 1: Science at the NCNR
Ronald Jones, Group Leader
Neutron Condensed Matter Science
2025 CHRNS Summer School

## Slide 2: What does the NCNR do?
NIST Mission
To promote U.S. innovation and industrial competitiveness by advancing measurement science, standards, and technology in ways that enhance economic security and improve our quality of life.
NCNR Mission
To advance economic and technical excellence in the U.S. by providing world-class neutron measurement capabilities to meet the needs of researchers from industry, academia, and government.

## Slide 3: Neutron Instruments at NCNR

## Slide 4: Neutron Instruments at NCNR
29 Beam Instruments
NCNR: 17 Scattering + test station
Physical Measurement Lab: 8
Material Measurement L: 3 + rabbits
BT4 3-Axis / FANS

## Slide 5: Broad Science Program
Engineering
T. Gnäupel-Herold et. al., Inconel 718 superalloy artifact
Rheo-SANS
R. Murphy, K. Weigandt, J. Krzywon, P. Butler, more…
Archaeology
R. Bishop et. al., Mayan trade routes
Neutron Physics
D. Sarenac et. al., Neutron Airy Beam
D
50 μm
Neutron Imaging
D. Hussey, J. LaManna, D. Jacobsen, others
Standard Reference Materials
N. Sharp, H. Chen-Mayer, M. Vega-Martinez, J. Weaver, C. Zangmeister

## Slide 6: Polymer Nanocomposites
Darvishi, Nazeer, Tyagi, Zhang, Narayanan, Kizilel, Senses
Macromolecules 54, 10118 (2021)
SANS
HFBS
Notes: For HFBS data, open circles are the neat material, and filled are PNCs with 30 vol % loading. HB = hyperbranched PEO.

## Slide 7: Aluminum Formate (ALF)
Hayden Evans, Craig Brown, Taner Yildirim; Cheetham Group, others
BT-1 Powder Diffractometer

## Slide 8: Aluminum Formate (ALF)
Hayden Evans, Craig Brown, Taner Yildirim; Cheetham Group, others
Gate opening mode: This gate opening mode controls the gas adsorption and desorption kinetics in ALF.
Quantum sieving up to 90 K (D2&H2 separation)
He confinement up to 80 K

## Slide 9: Aluminum Formate (ALF)
Hayden Evans, Craig Brown, Taner Yildirim; Cheetham Group, others

## Slide 10: Hybrid Skyrmions
Liyanage, Tang, Quigley, Borchers, Grutter, Maranville, Sinha, Reyren, Montoya, Fullerton, DeBeer-Schmitt, Gilbert - Phys. Rev. B 107, 184412
VSANS / CANDOR (PNR)
Notes: Fe (0.36 nm)/Gd (0.4 nm / Si

## Slide 11: Rheo - Spin Echo Neutron Spectroscopy
Gvaramia, Gutfreund, Falus, Faraone, Nagao, Wolff; Sci. Rep. 13, 13051 (2023)
Neutron Spin Echo / SANS
Notes: We compare the measured phase shift and depolarisation due to Doppler scattering from a rotating graphite disk to numerical and analytical calculations and find excellent agreement. This allows to take into account Doppler scattering during the data processing and makes longer Fourier times as well as higher shear rates and Q ranges possible with neutron spin echo spectroscopy, enabling for example the study of polymers under high shear.

## Slide 12: Uranium DiTelluride (UTe2)
Nick Butch, Sheng Ran, Silvia Lewin, Peter Czajka, Corey Frank, Tom Halloran, Gicela Saucedo Salas, UMD, MAGLAB, many others
Butch et al, npj Quantum Materials 7, 39 (2022)
MACS
Notes: INS: The temperature dependence of the low-energy magnetic excitations in the spin-triplet superconductor UTe2 was measured via inelastic neutron scattering in the normal and superconducting states. These excitations have a peak instensity at 4 meV, follow the Brillouin zone edges near the crystallographic b-axis, obey the paramagnetic structural symmetry, and track the temperature evolution of the heavy fermion bulk magnetic susceptibility. Thus, the imaginary part of the dynamic susceptibility follows the behavior of interband correlations in a hybridized Kondo lattice with an appropriate characteristic energy. These excitations are a lower-dimensional analog of phenomena observed in other Kondo lattice materials, such that their presence is not necessarily due to dominance of ferromagnetic or antiferromagnetic correlations. The onset of superconductivity alters the magnetic excitations noticeably on the same energy scales, suggesting that these changes originate from additional electronic structure modification.

## Slide 13: Time evolution of a pumped magnet
T. Reeder et al. PNAS, https://doi.org/10.1073/pnas.2415300121
Reveals different time scales in the dynamics of the Cr8 molecules when subjected to microwave pulses  resonant pumping produces a steady state that cannot be described by a conventional thermal equilibrium state
The tetragonal cell hosts two Cr8F8Piv16 molecules creating a staggered stacking of molecular square lattice planes
Continuous sample rotation
Magnetic field
Cryostat (temperature)
Square microwave pump
Event mode neutron detection
Map four-dimensional space
MACS
Notes: In postprocessing, the event mode data were binned into neutron counts versus scattering angle, sample rotation, energy transfer, and time relative to microwaves turning on. Such data were subsequently transformed into an event count map in a four-dimensional space d(Qx,Qy,hw,t) and the corresponding coverage map reporting the fission monitor count ħ associated with each pixel.

## Slide 14: Autonomous Formulation Lab (AFL)
github.com/usnistgov/AFL-agent
github.com/usnistgov/AFL-automation
github.com/usnistgov/AFL-hardware
Peter Beaucage, Donald Sutherland, Tyler Martin 10.1021/acs.macromol.4c01410

## Slide 15: Autonomous Formulation Lab (AFL)
Peter Beaucage, Jeff Krzywon, Tyler Martin, Donald Sutherland, Brad Sutliff, McGlynn; Dow Chemical, Diamond, ISIS

## Slide 16: ROADMAP
David Hoogerheide, Megan Mitchell, Frank Heinrich, Brian Maranville, Charles Majkrzak; others
Neutron reflectometry (NR)
Therapeutically relevant µM peptide concentrations
Membrane integrity (water content)
Surface peptide
Embedded peptide
Translocated peptide
Membrane thickness
CANDOR

## Slide 17: ROADMAP
David Hoogerheide, Megan Mitchell, Frank Heinrich, Brian Maranville, Charles Majkrzak; others
Bilayer
completeness

## Slide 18: What does the NCNR do?
NIST Mission
To promote U.S. innovation and industrial competitiveness by advancing measurement science, standards, and technology in ways that enhance economic security and improve our quality of life.
NCNR Mission
To advance economic and technical excellence in the U.S. by providing world-class neutron measurement capabilities to meet the needs of researchers from industry, academia, and government.