## Slide 1: Phase Identification Exercise
Using the Key Lines Table, identify the phase that produced each of these powder diffraction patterns using the phase identification table
Write your identifications in the table to the right
Mark the diagnostic peaks for each phase with an X
ID # | Phase
1 | 
2 | 
3 | 
4 | 
5 | 
6 | 
7 | 
9 | 
10 | 
11 | 
14 | 
15 | 
16 | 
18 | 
20 | 
21 | 
22 | 
23 | 
24 | 
25 | 
26 | 

## Slide 2: Key Lines for Cement Phase Identification using XRD
Bold type indicates a “diagnostic peak” for that phase, a peak that is relatively unaffected by overlaps from other phases
Keep in mind that this table (mostly) shows peaks with a relative intensity of 10 % or greater

## Slide 3: #1

## Slide 4: #2

## Slide 5
#3

## Slide 6
#4

## Slide 7
#5

## Slide 8
#6

## Slide 9
#7

## Slide 10
9

## Slide 11
10

## Slide 12
11

## Slide 13
13
Two Theta 14.63 | d-spacing 6.050 | Rel I 4
15.54 | 5.698 | 57
18.74 | 4.731 | 13
19.207 | 4.617 | 44
19.754 | 4.491 | 31
22.512 | 3.946 | 13
22.905 | 3.879 | 30
24.919 | 3.570 | 27
26.659 | 3.341 | 36
28.244 | 3.157 | 78
28.663 | 3.112 | 18
29.445 | 3.031 | 38
30.948 | 2.887 | 26
31.331 | 2.853 | 100
31.634 | 2.826 | 55
32.068 | 2.789 | 20
32.676 | 2.738 | 53
33.121 | 2.702 | 14
33.424 | 2.679 | 8
35.734 | 2.511 | 37
36.698 | 2.447 | 8
37.307 | 2.408 | 7
37.978 | 2.367 | 12
38.232 | 2.352 | 21
38.945 | 2.311 | 15
13

## Slide 14
14

## Slide 15
15

## Slide 16
16

## Slide 17
18

## Slide 18
20

## Slide 19
21

## Slide 20
22

## Slide 21
23

## Slide 22
24

## Slide 23
25

## Slide 24
26