## Slide 1: Neutron diffraction studies on the topologically non-trivial kagome helimagnet YMn6Sn6
NATIONAL INSTITUTE of STANDARDS and TECHNOLOGY ● NIST CENTER for NEUTRON RESEARCH
Rebecca L. Dally
NCNR, BT7 Instrument Scientist
CHRNS Summer School on Neutron Scattering
October 17 – 21, 2022

## Slide 2
NATIONAL INSTITUTE of STANDARDS and TECHNOLOGY ● NIST CENTER for NEUTRON RESEARCH
Acknowledgements
Synthesis, extensive bulk electronic and magnetic characterization (Ghimire lab @GMU,
M. A. McGuire @ORNL,
J.F. Mitchell & J. S. Jiang @Argonne)
Theory
(I. I. Mazin @GMU; M.P. Ghimire @Tribhuvan U.)
Neutron diffraction: SANS, triple-axis, & triple-axis polarized
(R.L. Dally, L. Poudel, M. Bleuel, J.W. Lynn @NCNR, K. Rule @ANSTO)
N. J. Ghimire et al, Sci. Adv. 6, eabe2680 (2020)
R. L. Dally et al, Phys. Rev. B 103, 094413 (2021)
P. E. Siegfried et al, Comm. Phys. 5, 58 (2022)

## Slide 3
NATIONAL INSTITUTE of STANDARDS and TECHNOLOGY ● NIST CENTER for NEUTRON RESEARCH
Why study Kagome lattice materials?
The RMn6Sn6 (HfFe6Ge6 structure) family and magnetic structures
YMn6Sn6 history and the B-T phase diagram
Topological Hall effect and the transverse conical spiral (TCS) magnetic phase
Polarized neutron results
Recent results: magnetoresistance and Ge-doped YMn6Sn6

## Slide 4
NATIONAL INSTITUTE of STANDARDS and TECHNOLOGY ● NIST CENTER for NEUTRON RESEARCH
L Ye et al. Massive Dirac fermions in a ferromagnetic kagome metal. Nature 555, 638–642 (2018) doi:10.1038/nature25987
Where to look for interesting physics in Kagome lattice materials

## Slide 5
NATIONAL INSTITUTE of STANDARDS and TECHNOLOGY ● NIST CENTER for NEUTRON RESEARCH
The RMn6Sn6 (HfFe6Ge6 structure) family contains many magnetic structures
HoFe6Ge6 structure (Immm)

## Slide 6
NATIONAL INSTITUTE of STANDARDS and TECHNOLOGY ● NIST CENTER for NEUTRON RESEARCH
The RMn6Sn6 (HfFe6Ge6 structure) family contains many magnetic structures
G. Venturini et al. J. Magn. Magn. Mater. 94(1–2), 35-42 (1991). https://doi.org/10.1016/0304-8853(91)90108-M

## Slide 7
NATIONAL INSTITUTE of STANDARDS and TECHNOLOGY ● NIST CENTER for NEUTRON RESEARCH
Timeline of key YMn6Sn6 research
1988
ternary stannide synthesis first reported for RMn6Sn6 (R = Sc, Y, Sm, Gd-Tm, Lu)
B. Malaman et al. Mater. Res. Bull. 23(11), 1629-1633 (1988). https://doi.org/10.1016/0025-5408(88)90252-8
1991
Crystal synthesis and bulk magnetic characterization revealing diversity of magnetic structures in RMn6Sn6 family
G. Venturini et al. J. Magn. Magn. Mater. 94(1–2), 35-42 (1991). https://doi.org/10.1016/0304-8853(91)90108-M
1996
Neutron diffraction revealed the (unusual) incommensurate antiferromagnetic spiral ground state of RMn6Sn6 (R = Sc, Y, Lu)
G. Venturini et al. J. Alloy Compd. 236(1–2), 102-110 (1996). https://doi.org/10.1016/0925-8388(95)01998-7

## Slide 8
NATIONAL INSTITUTE of STANDARDS and TECHNOLOGY ● NIST CENTER for NEUTRON RESEARCH
Timeline of key YMn6Sn6 research
2007
Bulk magnetic measurements with B ⟂ c published along with Hall data at 4.2 K
K. Uhlířová, et al. J. Magn. Magn. Mater. 310(2), 1747-1749 (2007). https://doi.org/10.1016/j.jmmm.2006.10.577
2020
Topological Hall effect (THE) found in transverse conical spiral magnetic phase. New THE mechansim proposed.
N. J. Ghimire et al, Sci. Adv. 6, eabe2680 (2020). https://doi.org/10.1126/sciadv.abe2680

## Slide 9
Zero-field magnetic structure is an antiferromagnet with incommensurate spiral order as the magnetic ground state
Centrosymmetric (P6/mmm)
Mn atoms form layers of kagome lattices with easy-plane anisotropy
Mn layer above not the same distance as layer below
  need J1-J2-J3 interlayer exchange interaction model
  Jp<0, J1<0, J2>0, J3<0
  frustrated magnet
NATIONAL INSTITUTE of STANDARDS and TECHNOLOGY ● NIST CENTER for NEUTRON RESEARCH

## Slide 10
NATIONAL INSTITUTE of STANDARDS and TECHNOLOGY ● NIST CENTER for NEUTRON RESEARCH
Magnetic structures in the in-plane B-T phase diagram

## Slide 11
NATIONAL INSTITUTE of STANDARDS and TECHNOLOGY ● NIST CENTER for NEUTRON RESEARCH
Magnetic structures in the in-plane B-T phase diagram
k1 = (0, 0, 0), k2 = (0, 0, 0.5)
γ = 52(2)◦, µ = 1.13(4)µB

## Slide 12
NATIONAL INSTITUTE of STANDARDS and TECHNOLOGY ● NIST CENTER for NEUTRON RESEARCH
Magnetic structures in the in-plane B-T phase diagram
k1 = (0, 0, 0), k2 = (0, 0, 0.25), k3 = (0, 0, 0.5)
γ = 68(2)◦ , δ = 0(1)◦ , µ = 1.95(5)µB

## Slide 13
NATIONAL INSTITUTE of STANDARDS and TECHNOLOGY ● NIST CENTER for NEUTRON RESEARCH
Magnetic structures in the in-plane B-T phase diagram
k1 = (0, 0, kz), k2 = (0, 0, 0)
“Phase I” incommensurate

## Slide 14
The zero-field magnetic structure is a commensurate AFM at TN and quickly transforms to an incommensurate double-flat-spiral
Sn2Y
Sn3
TN ~ 340 K, k = (0, 0, 0.5)
NATIONAL INSTITUTE of STANDARDS and TECHNOLOGY ● NIST CENTER for NEUTRON RESEARCH

## Slide 15
NATIONAL INSTITUTE of STANDARDS and TECHNOLOGY ● NIST CENTER for NEUTRON RESEARCH
The zero-field magnetic structure is a commensurate AFM at TN and quickly transforms to an incommensurate double-flat-spiral
TIC ~ 330 K, k = (0, 0, kz)
actually k1 = (0, 0, kz,1) and k2 = (0, 0, kz,2)

## Slide 16
NATIONAL INSTITUTE of STANDARDS and TECHNOLOGY ● NIST CENTER for NEUTRON RESEARCH
1
2
3
4
5
6
Magnetic ground state structure in zero field is the incommensurate double spiral structure [Venturini, et al. J Alloy Compd 236(1-2), 102-110 (1996).]

## Slide 17
NATIONAL INSTITUTE of STANDARDS and TECHNOLOGY ● NIST CENTER for NEUTRON RESEARCH
Unpolarized neutrons cannot distinguish chirality
Example:
because
Two chiral domains possible

## Slide 18
NATIONAL INSTITUTE of STANDARDS and TECHNOLOGY ● NIST CENTER for NEUTRON RESEARCH
Polarized neutrons can distinguish chirality: scattering amplitude modified to consider initial and final spin states of neutron
sample
Four cross sections: , , ,

## Slide 19
NATIONAL INSTITUTE of STANDARDS and TECHNOLOGY ● NIST CENTER for NEUTRON RESEARCH
Polarized neutrons can distinguish chirality: scattering amplitude modified to consider initial and final spin states of neutron
Four cross sections: , , ,
For polarization parallel to , magnetic scattering is spin-flip i.e. or

## Slide 20
NATIONAL INSTITUTE of STANDARDS and TECHNOLOGY ● NIST CENTER for NEUTRON RESEARCH
Polarized neutrons can distinguish chirality: scattering amplitude modified to consider initial and final spin states of neutron
Four cross sections: , , ,
For polarization parallel to , magnetic scattering is spin-flip i.e. or

## Slide 21
NATIONAL INSTITUTE of STANDARDS and TECHNOLOGY ● NIST CENTER for NEUTRON RESEARCH
Polarized neutrons can distinguish chirality: scattering amplitude modified to consider initial and final spin states of neutron
Intensity

## Slide 22
NATIONAL INSTITUTE of STANDARDS and TECHNOLOGY ● NIST CENTER for NEUTRON RESEARCH
Polarized neutrons can distinguish chirality: scattering amplitude modified to consider initial and final spin states of neutron
Intensity
Intensity

## Slide 23
NATIONAL INSTITUTE of STANDARDS and TECHNOLOGY ● NIST CENTER for NEUTRON RESEARCH
Polarized neutrons can distinguish chirality: scattering amplitude modified to consider initial and final spin states of neutron
Intensity
Intensity

## Slide 24
NATIONAL INSTITUTE of STANDARDS and TECHNOLOGY ● NIST CENTER for NEUTRON RESEARCH
Polarized neutron diffraction data show an imbalance of the positive vs negative chiral domains despite centrosymmetric structure

## Slide 25
NATIONAL INSTITUTE of STANDARDS and TECHNOLOGY ● NIST CENTER for NEUTRON RESEARCH
Helimagnetism in centrosymmetric YMn6Sn6 due to frustrated interlayer exchange, should not see chiral imbalance
Possible control of spin helicity?
MnP

## Slide 26
NATIONAL INSTITUTE of STANDARDS and TECHNOLOGY ● NIST CENTER for NEUTRON RESEARCH
topological Hall effect arises from charges moving through a spatially varying magnetic field: chiral and non-coplanar spin configuration required.
Yokouchi T. Springer Theses (2019). https://doi.org/10.1007/978-981-32-9385-4_1
static scalar spin chirality
Observation of topological Hall effect indicates an underlying topologically protected spin structure
robust phase

## Slide 27
NATIONAL INSTITUTE of STANDARDS and TECHNOLOGY ● NIST CENTER for NEUTRON RESEARCH
When a magnetic field is applied in-plane, there are many new magnetic phases. The topological Hall effect was observed in one of these phases at elevated temperatures.

## Slide 28
NATIONAL INSTITUTE of STANDARDS and TECHNOLOGY ● NIST CENTER for NEUTRON RESEARCH
Neutron diffraction work at NCNR showed the topological Hall effect coincided with a transverse conical spiral (TCS) magnetic structure
double spiral to transverse conical spiral
H
~50% reduction in neutron intensity

## Slide 29
NATIONAL INSTITUTE of STANDARDS and TECHNOLOGY ● NIST CENTER for NEUTRON RESEARCH
All the other structures in the magnetic phase diagram were identified via neutron diffraction
DS
(distorted spiral)
double spiral
TCS
(transverse conical spiral)
FL
(fan-like)
FF
(forced ferromagnet)

## Slide 30
NATIONAL INSTITUTE of STANDARDS and TECHNOLOGY ● NIST CENTER for NEUTRON RESEARCH
The elevated temperatures of the topological Hall effect along with the null scalar spin chirality indicated thermal fluctuations of the magnons are playing a part
Nakata et al. J. Phys. D: Appl. Phys. 50 114004 (2017).

## Slide 31
NATIONAL INSTITUTE of STANDARDS and TECHNOLOGY ● NIST CENTER for NEUTRON RESEARCH
The elevated temperatures of the topological Hall effect along with the null scalar spin chirality indicated thermal fluctuations of the magnons are playing a part

## Slide 32
NATIONAL INSTITUTE of STANDARDS and TECHNOLOGY ● NIST CENTER for NEUTRON RESEARCH

## Slide 33
NATIONAL INSTITUTE of STANDARDS and TECHNOLOGY ● NIST CENTER for NEUTRON RESEARCH

## Slide 34
NATIONAL INSTITUTE of STANDARDS and TECHNOLOGY ● NIST CENTER for NEUTRON RESEARCH
The interlayer magnetic interactions coupled with an applied magnetic field in the ab-plane lead to a complex and multi-magnetic structure B-T phase diagram

## Slide 35
NATIONAL INSTITUTE of STANDARDS and TECHNOLOGY ● NIST CENTER for NEUTRON RESEARCH
Polarized neutron scattering revealed an imbalance between the positive and negative chiral domain population

## Slide 36
NATIONAL INSTITUTE of STANDARDS and TECHNOLOGY ● NIST CENTER for NEUTRON RESEARCH
The elevated temperatures of the topological Hall effect along with the null scalar spin chirality indicate thermal fluctuations of the magnons are playing a part

## Slide 37
NATIONAL INSTITUTE of STANDARDS and TECHNOLOGY ● NIST CENTER for NEUTRON RESEARCH
Recent developments for our YMn6Sn6 research: magnetotransport reveals two types of Lifshitz transitions
P. E. Siegfried et al, Comm. Phys. 5, 58 (2022)
Driven by a continuously changing magnetization (rare) (H`)
Electron-spin coupling driven, without large SOC (H2)

## Slide 38
NATIONAL INSTITUTE of STANDARDS and TECHNOLOGY ● NIST CENTER for NEUTRON RESEARCH
Recent developments for our YMn6Sn6 research: magnetotransport reveals two types of Lifshitz transitions
Driven by a continuously changing magnetization (rare) (H`)
Electron-spin coupling driven, without large SOC (H2)

## Slide 39
NATIONAL INSTITUTE of STANDARDS and TECHNOLOGY ● NIST CENTER for NEUTRON RESEARCH
Recent developments for our YMn6Sn6 research: magnetotransport reveals two types of Lifshitz transitions
Driven by a continuously changing magnetization (rare) (H`)
Electron-spin coupling driven, without large SOC (H2)

## Slide 40
NATIONAL INSTITUTE of STANDARDS and TECHNOLOGY ● NIST CENTER for NEUTRON RESEARCH
Recent developments for our YMn6Sn6 research: Ge-doped neutron diffraction
YMn6Sn6-xGex (x ≈ 1.8)
Ge preferentially goes into Y layer
Magnetization measurements show similar µ0H-T phase diagram to parent but points to absence of TCS phase
YMn6Ge6 is a commensurate c-axis antiferromagnet at RT and undergoes a commensurate-incommensurate transition below 80 K to a c-axis cone antiferromagnetic structure (easy-axis)
G. Venturini et al. J. Alloy Compd. 200(1–2),51-57 (1993).

## Slide 41
NATIONAL INSTITUTE of STANDARDS and TECHNOLOGY ● NIST CENTER for NEUTRON RESEARCH
Recent developments for our YMn6Sn6 research: Ge-doped neutron diffraction
TN = 348 K
No high temperature commensurate phase found
Two wavevectors still present with ki = (0, 0, kz,i) (i = 1,2)

## Slide 42
NATIONAL INSTITUTE of STANDARDS and TECHNOLOGY ● NIST CENTER for NEUTRON RESEARCH
Recent developments for our YMn6Sn6 research: Ge-doped neutron diffraction
Mn-Mn d1
Mn-Mn d2
 | YMn6Sn6 | YMn6Sn6-xGex (x ≈ 1.84)
Mn-Mn in-plane | 2.767 Å (FM) | 2.700 Å
Mn-Mn d1 | 4.552 Å (FM) | 4.644 Å
Mn-Mn d2 | 4.458 Å (AFM) | 4.036 Å

## Slide 43
NATIONAL INSTITUTE of STANDARDS and TECHNOLOGY ● NIST CENTER for NEUTRON RESEARCH
Recent developments for our YMn6Sn6 research: Ge-doped neutron diffraction

## Slide 44
NATIONAL INSTITUTE of STANDARDS and TECHNOLOGY ● NIST CENTER for NEUTRON RESEARCH
Recent developments for our YMn6Sn6 research: Ge-doped neutron diffraction

## Slide 45
NATIONAL INSTITUTE of STANDARDS and TECHNOLOGY ● NIST CENTER for NEUTRON RESEARCH
k = (0, 0, kz)
kz ~ 0.23 (0 T) – 0.24 (6 T)
k = (0, 0, kz)
kz ~ 0.18

## Slide 46
NATIONAL INSTITUTE of STANDARDS and TECHNOLOGY ● NIST CENTER for NEUTRON RESEARCH
Thank you for your attention!
Ghimire et al. Science Advances, 6, 51, eabe2680 (2020). DOI: 10.1126/sciadv.abe2680
Dally et al. Physical Review B, 103, 094413 (2021). DOI: 10.1103/PhysRevB.103.094413
P. E. Siegfried et al, Comm. Phys. 5, 58 (2022). https://doi.org/10.1038/s42005-022-00833-2