- Service Life Prediction for Concrete Pavements and Bridge Decks Exposed to Sulfate Attack and Freeze-Thaw Deterioration, Volume II: Technical Basis for CONCLIFE: Sorptivity Testing and Computer Models

- Dale P. Bentz

Chiara F. Ferraris

John Winpigler

Building and Fire Research Laboratory

National Institute of Standards and Technology

Gaithersburg, MD 20899

- ABSTRACT

This report provides the technical background for the CONCLIFE software package developed at the National Institute of Standards and Technology.  CONCLIFE estimates the service life of concrete pavements and bridge decks exposed to sulfate attack and freeze/thaw deterioration, where the major transport mechanism for water and sulfate ion ingress is sorption by partially saturated concrete.  This report supplements the CONCLIFE User’s Guide by providing details on the laboratory testing to evaluate the sorptivity of concrete cylindrical cores obtained from field specimens and the three underlying computer models used by CONCLIFE in obtaining service life estimates.  This report is volume II of a two-part series.  Volume I is the user’s manual for the developed CONCLIFE software package.

Keywords: building technology, concrete bridge decks, concrete pavements, environmental conditions, freeze-thaw deterioration, service life, sorptivity, sulfate attack.

TABLE OF CONTENTS

Section										 	   Page

CHAPTER 1: INTRODUCTION	1

CHAPTER 2: SORPTIVITY TESTING	3

2.1 Materials	3

2.2 Methodology Development	8

2.2.1 Conditioning of the Specimens	8

2.2.2 Sorptivity Test	10

2.2.3 Results	14

2.2.4 Standardization Efforts	15

CHAPTER 3: COMPUTER MODELS	17

3.1 Concrete Surface Temperature and Time of Wetness (Heat Transfer Model)	17

3.2 Sulfate Attack	21

3.3 Freeze/thaw Damage	22

CHAPTER 4: SUMMARY	25

ACKNOWLEDGEMENTS	26

REFERENCES	27

APPENDIX A: ASTM CXXXX Proposed Test Method for Measurement of Rate of Absorption of Water by Hydraulic-Cement Mortars or Concretes	29

1.	Scope	29

2.	Referenced Documents	29

3.	Significance and Use	29

4.	Apparatus	30

5.	Reagents and Materials	31

6.	Test Specimens	32

7.	Sample Conditioning	32

8.	Procedure	33

9.	Calculations	36

10.	Report	37

11.	Precision and Bias	38

APPENDIX 1:Example Rate of Absorption Test	39

LIST OF FIGURES

Figure												   Page

Figure 1: Relative Humidity achieved after the various pre-conditionings. The main difference is the duration spent in the environmental chamber at 50 C and 80% RH. T1: no time; T2: 24h; T3: 48 h; T4: 3 d; T5: 7d; T6: until constant mass; T7: until constant mass at 20 C and 80% RH. The right scale is not identical to the left scale for better visualization of the average curve.	8

Figure 2: RH of the air inside the conditioning jars versus time.	9

Figure 3: Comparison of sorption measured by capillary and by ponding. A) The water content per surface area versus linear time as measured; B) the water content per surface area vs. square root of time for the first 7 hours.	10

Figure 4: Schematic of the capillary sorption test.	11

Figure 5: Schematic of the ponding sorption test.	11

Figure 6: Pictures of observed leaks with the incorrect tape.  A) the water is leaking between the two layer of tape; B) the water has leaked in between the tape and the specimen sides and is wetting the bottom (non tested surface).	12

Figure 7: Calculation of the sorption coefficient.	13

Figure 8. Basic configuratins of one-dimensional heat transfer models for concrete pavements and bridge decks.	16

Figure 9. Temperature predictions for a concrete pavement in Providence, Rhode Island in the spring.  Time indicates cumulative hours from beginning of year.	18

Figure 10. Plots of wetting events in (top) Kansas City, MO and (bottom) Providence, RI, both for concrete pavements.	19

Figure 11. Schematic of Procedure A.	30

Figure 12. Schematic of Procedure B.	32

LIST OF TABLES

Table												   Page

Table 1: Mix design and concrete properties for the specimens from the Virginia DOT.  All the data were provided by the DOT and were not remeasured at NIST.	4

Table 2: Mix design and concrete properties for the specimens from the Maryland DOT.  All the data were provided by the DOT and were not remeasured at NIST.	5

Table 3: Mix design and concrete properties for the specimens from the Missouri DOT.  All the data were provided by the DOT and were not remeasured at NIST.	6

Table 4: Mix design and concrete properties for the specimens from the Rhode Island DOT.  All the data were provided by the DOT and were not remeasured at NIST.	7

Table 5: Modulus of elasticity for the concretes.	7

Table 6: Sorptivity properties for the concretes. Only one specimen was available from each type, therefore no error analysis is possible.	14

Table 7. Generic mterial properties for the heat transfer model.	18

# CHAPTER 1: INTRODUCTION

CONCLIFE is a Windows-based software package for estimating the expected service lives of concrete pavements and bridge decks, considering transport due to sorption and degradation due to either sulfate attack or freeze/thaw damage.  While a separate user’s guide for the CONCLIFE software has recently been published,(1) the purpose of this supplemental document is to describe the underlying technical basis for the CONCLIFE software.  A standard test method for evaluating the sorptivity coefficients of a concrete is a pre-requisite to any sorptivity-based predictions of service life.  Thus, the next chapter of this report deals with the technical basis for the development of a standard concrete sorptivity test.(2)  The third chapter provides a description of the various computer models employed in CONCLIFE, both those used to estimate concrete surface temperature and time-of-wetness, and those used to estimate degradation due to either sulfate attack or freeze/thaw deterioration.

# CHAPTER 2: SORPTIVITY TESTING

To develop a test to measure the rate of ingress of water in concrete specimen, there are two approaches: 1) in-situ testing, i.e., the concrete is tested in place in the field; 2) laboratory testing, i.e., concrete cores are taken and brought to a laboratory for testing.  Both approaches have their advantages and disadvantages.  In the in-situ approach, the concrete cannot be easily conditioned and it is thus not possible to know the water content of the concrete, which has a large effect on measured transport properties.(3)  In the laboratory approach, the concrete might not be exactly the “same” as the in-situ concrete, i.e., curing, hydration degree, etc., if, for example, substantial time elapses between obtaining the cores and testing them.  Nevertheless, the goal of the test is to determine the properties of the in-situ concrete.

The approach selected here is laboratory testing because we felt that a higher reliability could be achieved.  The data will give a good estimate of the material properties that can then be used to model the performance of the in-situ concrete as a function of the environment.

## 2.1 Materials

To develop the sorptivity test, cores from either the actual construction or from in-situ specially cast specimens, or cast cylinders were used.  The specimens were provided to us by the following state departments of transportation (DOTs): Virginia, Maryland, Missouri, and Rhode Island.  The sets received from Virginia and Maryland were used to develop the conditioning methodology.  The other two sets were used for finalizing the sorptivity test methodology using the ponding option.

The following tables (table 1 to table 4) give the mix designs of the various specimens received.  The specimens received from Maryland and from Virginia were cast cylinders from the same concrete as the main structure at the construction site.

The specimens received from the Rhode Island DOT were cores from small slabs (610 mm x 610 mm x 914 mm deep or 2 ft x 2 ft by 3 ft).  The slabs were prepared by pumping the concrete into the molds.  The slabs were then field cured and the cores were obtained after 28 d of curing.  The cores were 368 mm (14.5 in) in length and 100 mm (4 in) in diameter.  The specimens received from the Missouri DOT were cores from actual pavement slabs, not from separately cast specimens.  These were taken from Route 65 in Benton County and from Route 13 in Henry County.  The cores were from both the driving lanes (DL) and the passing lanes (PL) and were all from the northbound direction of the road.

Table 1: Mix design and concrete properties for the specimens from the Virginia DOT.  All the data were provided by the DOT and were not remeasured at NIST.

|  | MIX #1 (FHWA-72 A/C) | Mix #2 (FHWA-72 D/F) |
| --- | --- | --- |
| Date | 7/7/99 | 6/30/99 |
| Mixture Proportions |  |  |
| Cement kg/m3 (lb/yd3) | 234 (395) | 251 (423) |
| Slag kg/m3 (lb/yd3) | 100 (169) |  |
| Fly Ash kg/m3 (lb/yd3) |  | 84 (141) |
| Pozzolan (mass %) | 30 | 25 |
| Coarse aggregates (No. 57) kg/m3 (lb/yd3) | 1092 (1840) | 1092 (1840) |
| Fine Aggregates kg/m3 (lb/yd3) | 722 (1217) | 729 (1229) |
| Water kg/m3 (lb/yd3) | 148 (250) | 148 (250) |
| W/cm | 0.44 | 0.44 |
| Admixtures | AEA | AEA |
| Concrete Properties |  |  |
| Slump mm (in) | 63.5 (2.5) | 38.1 (1.5) |
| Air content (%) | 5.0 | 4.2 |
| Concrete temperature C (F) | 30.5 (87) | 28 (82) |
| Compressive strength MPa (psi) at 28 days on cylinders 152 mm x 508 mm (6 in x 20 in) | 36.5 (5300) | 33.9 (4920) |
| Flexural strength MPa (psi) at 28 d on prisms 152 mm x 152 mm x 508 mm (6 in x 6 in x 20 in) | 5.4 (785) |  |
| Rapid Chloride Permeability at 28 d (ASTM C1202) | 1584 | 700 |
| Curing | Moist cured at 23 C for 7 d followed by moist curing at 38C for 21 d and testing at 28 d Kept in plastic molds with the same curing as 1) |  |
| Shipped and further curing | Shipped in plastic bags or in their original molds; received by NIST on 8/17/99; At NIST, the specimens were stored in limewater until testing, if received in bags; in their molds in a moist cabinet until testing, if received in molds |  |

Table 2: Mix design and concrete properties for the specimens from the Maryland DOT.  All the data were provided by the DOT and were not remeasured at NIST.

|  | MIX #1 (FHWA-68) |
| --- | --- |
| Date | 3/2/99 |
| Mixture Proportions |  |
| Cement kg/m3 (lb/yd3) | 262 (442) |
| Newcem kg/m3 (lb/yd3) | 141 (238) |
| Pozzolan (mass %) | 35 |
| Coarse aggregates (No. 57) kg/m3 (lb/yd3) | 1080 (1820) |
| Fine Aggregates kg/m3 (lb/ft3) | 688 (1160) |
| Water kg/m3 (lb/ft3) | 158 (267) |
| W/cm | 0.39 |
| Admixtures | AEA and HRWRA |
| Concrete Properties |  |
| Slump mm (in) | 50-127 (2-5) |
| Air content (%) | 6.5 |
| Concrete temperature C (F) | Not measured |
| Designed Compressive strength MPa (psi) at 28 days | 31 (4500) |
| Rapid Chloride Permeability at 28 d (ASTM C1202) | Not measured |
| Curing | Moist cured at 23 C until pick up date |
| Shipped and further curing | Picked up on 7/21/99; transported in plastic bags with wet burlaps; At NIST, the specimens were stored in limewater until testing. |

Table 3: Mix design and concrete properties for the specimens from the Missouri DOT.  All the data were provided by the DOT and were not remeasured at NIST.

|  | Route 65 (FHWA-152/154) | Route 13 (FHWA-153) |
| --- | --- | --- |
| Date cast | 06/29/00 | 06/29/00 |
| Date Core taken | 07/26/00 | 07/25/00 |
| Mixture Proportions |  |  |
| Cement kg/m3 (lb/yd3) | 290 (488) | 251 (423) |
| Fly Ash kg/m3 (lb/yd3) | 51 (86) |  |
| Pozzolan (mass %) | 15 | 0 |
| Coarse aggregates (Limestone) kg/m3 (lb/yd3) | 1069 (1801) | 992 (1672) |
| Fine Aggregates kg/m3 (lb/yd3) | 586 (988) | 729 (1038) |
| Water kg/m3 (lb/yd3) | 123 (207) | 88 (148) |
| W/cm | 0.36 | 0.35 |
| Admixtures | AEA (73 L/m3) |  |
| Concrete Properties |  |  |
| Slump mm (in) | 30.5 (1.2) | (44.5) 1.75 |
| Air content (%) | 5.0 | 4.2 |
| Concrete temperature C (F) | 27 (80) | 28 (82) |
| Curing | In situ |  |
| Shipped and further curing | Shipped in plastic bags; received by NIST on 8/2/00; At NIST, the specimens were stored in limewater until testing. |  |

Table 4: Mix design and concrete properties for the specimens from the Rhode Island DOT.  All the data were provided by the DOT and were not remeasured at NIST.

|  | MIX #1 (FHWA-150) |
| --- | --- |
| Date cast | 6/14/00 |
| Mixture Proportions |  |
| Cement kg/m3 (lb/yd3) | 417 (703) |
| Coarse aggregates (3/4” and pea stones) kg/m3 (lb/yd3) | 1054 (1776) |
| Fine Aggregates kg/m3 (lb/ft3) | 681 (1148) |
| Water kg/m3 (lb/ft3) | 163 (275) |
| W/cm | 0.39 |
| Admixtures | DCI (15 L/m3) |
| Concrete Properties: none available |  |
| Curing | Unknown |
| Shipped and further curing | Received on 7/31/00. At NIST, the specimens were stored in limewater until testing; |

For the specimens from Missouri and Rhode Island, the elastic moduli were measured based on the resonance frequency method as described in ASTM C 215.(4)  The mode used was longitudinal, i.e., the accelerometer was on the same axis as the driver.  The values obtained, along with their measured standard deviations, are given in table 5.  It is interesting to notice that the driving lane has systematically higher values than the passing lane. We have no explanation for this phenomenon. More information on the casting pattern, the curing or any other differences in the treatment or the materials used needs to be available in order to attempt to explain the difference.

- Table 5: Modulus of elasticity for the concretes.

| Rhode Island | Missouri Rt.65 |  | Missouri Rt. 13 |  |
| --- | --- | --- | --- | --- |
|  | Driving lane | Passing Lane | Driving Lane | Passing lane |
| 44  1 GPa | 46  0.3 GPa | 42  0.2 GPa | 48  0.3 GPa | 43  0.2 GPa |

## 2.2 Methodology Development

### 2.2.1 Conditioning of the Specimens

To develop a laboratory test to measure sorptivity, two main hurdles needed to be overcome: 1) the conditioning of the specimen; and 2) the test itself.

As the sorptivity depends strongly on the water saturation of the concrete, the conditioning of the specimen is paramount.  Therefore, the requirements for a good conditioning procedure for the specimens should include:

- Equilibrium with the same relative humidity should be achieved with any concrete;

- The relative humidity (RH) in equilibrium with the specimen should be around 60 percent, because it is a likely limit on the lowest relative humidity encountered in the field;

- The duration of the conditioning should be as short as possible;

- The methodology should not require sophisticated instrumentation. This will allow the implementation of the test by most laboratories.

Therefore, the more severe conditioning consisting of drying the specimen to constant mass in an oven was rejected a priori.  On the average, a concrete specimen 100 mm in diameter and 50 mm in length will need some 2-3 months to be completely oven dried.  This duration is not acceptable.  The methodology adopted to determine the optimum conditioning was:

- Vacuum saturate the specimen as described in ASTM C1202;(5)

- Place the specimens in an environmental chamber at 80 percent RH and 50 C. The duration of this treatment should be the shortest possible to obtain the same equilibrium RH with all concretes

- Place the specimen in a closed container at 20 C until the specimen has the same RH throughout its thickness. The RH of the air in the container was monitored to determine the equilibrium.

Therefore, the first point to determine was the duration of the treatment in the environmental chamber to obtain a consistent RH for all specimens. The procedure to determine the duration was to expose concrete specimens obtained from the DOTs to various durations of exposure and measure the RH after two weeks. The goal was to obtain a similar RH for all specimens. The durations selected were:

- T1: No time in the environmental chamber. The specimens were directly placed in closed containers after being vacuum saturated

- T2: 24 h

- T3: 48 h

- T4: three d

- T5: seven d

- T6: the specimens were kept in the environmental chamber until they achieved constant mass. The duration was on the order of three to four months depending on the specimen.

- T7: the specimen was kept in the environmental chamber until it achieved constant mass but the temperature of the chamber was changed to 20 C.

Figure 1 shows the results obtained.  Each result represented on the bar chart is the average of two specimens.  The bars show the influence of the mixture design on the final RH achieved, while the line plot shows the average for all specimens in any mixture design for a given conditioning.  The goal is to obtain the conditioning that results in the smallest variation between the specimens.  It is clear that the conditioning from T3 and higher are acceptable, with the unexplained exception of T4.  Therefore, we suggest that the specimens should be kept in the environmental chamber for at least 48 h prior to placement in the container to equilibrate the RH.  Of course the smallest variation between specimens is obtained when constant mass is achieved (conditions T6 and T7), but the duration of the conditioning is not acceptable for a standard test.

Figure 1: Relative Humidity achieved after the various pre-conditionings. The main difference is the duration spent in the environmental chamber at 50 C and 80% RH. T1: no time; T2: 24h; T3: 48 h; T4: 3 d; T5: 7d; T6: until constant mass; T7: until constant mass at 20 C and 80% RH. The right scale is not identical to the left scale for better visualization of the average curve.

The second step that needs to be addressed is the duration of the conditioning of the specimen in a closed container to obtain a uniform RH throughout the specimen.  To determine the shortest duration needed, specimens were placed in special containers.  These containers were wide mouth jars with a metal lid.  The mouth of the jars was wide enough to accommodate the placement of the specimen inside the jar.  Two valves were attached to the lid.  These valves open only when a male connection is attached to them.  A dew point hygrometer was used to measure the RH inside the jars.  It was connected regularly to each jar through the one way valves in the lids of the jars.  The RH was monitored once a day for at least two weeks.  Figure 2 shows the evolution of the RH versus time.  It can be deduced that after about 10 days the RH does not changes significantly.  Therefore, the duration adopted was 15 days to guarantee a uniform RH throughout the specimen.

- Figure 2: RH of the air inside the conditioning jars versus time.

### 2.2.2 Sorptivity Test

Water ingress into a non-saturated concrete structure is due to sorption, driven by capillary forces.(3)  If the water is on top of the concrete surface, gravity also will play a role in the water penetration.  Figure 3 shows the different results obtained with the two methods: capillary (against gravity) or ponding (with gravity).  It is clear that the specimens have a higher water intake by ponding than by capillary transport alone.  Therefore, it is necessary to use the method more appropriate for the application of the concrete structure to be evaluated.  The determined sorptivity coefficients are 0.4910-3 m/√s for the capillary sorption and 0.5910-3 m/√s for the ponding sorption for the data presented in figure 3.

To measure the sorption coefficient of concrete, a new test proposed by NIST to ASTM for standardization was used.(2)  The method is similar to that recently published as a RILEM recommendation.(6)  The principle of the method is that a concrete specimen has one surface in contact with water while all others are sealed.

Figure 3: Comparison of sorption measured by capillary and by ponding. A) The water content per surface area versus linear time as measured; B) the water content per surface area vs. square root of time for the first 7 hours.

The proposed standard test allows either the top surface to be in contact (simulation of water on a pavement or bridge deck) or the bottom surface (substrate in contact with water).  The first case is referred to as ponding sorption and the second as capillary sorption.

The concrete specimens were 50 mm (2 in) thick disks sliced from the received specimens.  The sides were covered with duct tape prior to the pre-conditioning, in order to treat all specimens equally prior to the initial vacuum saturation procedure used in this study.  By contrast, in the draft ASTM standard provided in the Appendix, the specimens are sealed (taped) after the pre-conditioning and just prior to actual testing.  This should somewhat reduce the time necessary to reach moisture equilibrium within the specimen.

In both cases, the surface not tested was covered with a plastic wrap secured with a rubber band or an equivalent system.  In the case of capillary sorption (Figure 4) the specimens were then ready for testing.  For ponding sorption, some duct tape was used to form a pool (dike) as shown in Figure 5.  A two-component epoxy caulk was used to seal the space between the tape and the concrete.

The mass of the specimen was then regularly measured after the tested surface was patted dry. Of course, in the case of ponding, the water inside the dike needed to be poured out before patting dry the surface.

- Figure 4: Schematic of the capillary sorption test.

- Figure 5: Schematic of the ponding sorption test.

It should be mentioned that the tape used in these tests needs to be evaluated to avoid leaks.  These leaks will be deleterious to obtaining correct results, especially in the ponding configuration.  Figure 6 shows the possible cases of leakage that can alter the validity of the results: the water leaks between the two sides of the tape or between the tape and the specimen and wets the non-testing surface.  In both cases, the results will show a higher sorption coefficient than the correct value.

To select the correct tape and caulk, one can use any concrete cylinder as a “dummy” specimen. The steps to follow are:

- Dry the specimen somewhat by placing it in an oven overnight,

- Prepare the specimen for the ponding tests as described above and use the tape to be tested

- Pour water in the dike and leave the specimen overnight.

In general, if the tape is not adequate, the leaks will appear in less than 24 h.  It would have been more scientific to develop a clear criteria for determining the “stickiness” of the tape, but it was beyond the scope of this project.  Some valuable information on selecting an appropriate tape can be found in a guide to tapes for use in backpacking.(7)

Figure 6: Pictures of observed leaks with the incorrect tape.  A) the water is leaking between the two layer of tape; B) the water has leaked in between the tape and the specimen sides and is wetting the bottom (non tested surface).

To determine the sorption coefficient, the mass gain divided by the surface area of the top surface is plotted versus the exposure time. The sorption coefficients are defined as shown in the following equation:

WρA=St+I0		(1)

where

W = mass gain (kg)

A= surface are tested [m2]

t = time variable [min]

S  = early age sorption coefficient [mm/min1/2]  if 1 min < t < 7 h

later age sorption coefficient [mm/min1/2]  if t > 1 d

I0 = initial sorption (mm)

ρ = density of water (kg/m3)

Figure 7 shows these two slopes or sorption coefficients.  Two slopes have been observed for the results obtained from a wide variety of concretes and mortars.(8)  The later age sorption coefficient is usually attributed to other phenomena besides the capillary forces alone, such as filling of the larger pores and air voids.  The nick-point time is defined as the time where the lines with the two slopes cross as shown in figure 7.

- Figure 7: Calculation of the sorption coefficient.

### 2.2.3 Results

Many tests were conducted to develop the test using many of the specimens described above.  Here, we have selected to only present the data obtained in ponding sorption for the concretes from Rhode Island and from Missouri, as these tests were performed after the methodology was well established.

- Typical measured sorptivity values for the three concretes (following the seven d environmental chamber conditioning regime) are provided in Table 6.  The concrete from Rhode Island is seen to exhibit a rapid initial sorption relative to the two concretes from Missouri (as seen in the values of I0).  After this initial absorption, the values of S(early age) for the three concretes are seen to be very similar (a coefficient of variation between the three samples of  only 13 percent).  The values of S(later age) exhibit a much higher variability between the three concretes (coefficient of variation of  60 percent).

Table 6: Sorptivity properties for the concretes. Only one specimen was available from each type, therefore no error analysis is possible.

| - Sorption Property | - Rhode Island | - Missouri Rte 65 Driving Lane | - Missouri Rte 13 Driving Lane |
| --- | --- | --- | --- |
| - I0 (early age) (mm) | - 5.46 | - 0.075 | - 0.017 |
| - S (early age) (10-3 mm/√min) | - 2.79 | - 3.25 | - 3.64 |
| - Nick point time (h) | - 7 | - 7 | - 6 |
| - I0 (later age) (mm) | - 5.34 | - 0.065 | - 0.034 |
| - S (later age) (10-3 mm/√min) | - 8.98 | - 3.95 | - 3.02 |

### 2.2.4 Standardization Efforts

Based on previous drafts prepared by Prof. Doug Hooton of the University of Toronto, the sorption coefficient test was updated and presented to ASTM Committee C09.(2)  The first ballot has been completed and the comments from the committee members have been introduced into a revised draft.  This revised draft (provided in Appendix A) was sent for discussion to the members, prior to the June 2001 meeting.  A precision and bias statement is currently being developed and will be presented at the December 2001 ASTM C09 meeting for balloting.

# CHAPTER 3: COMPUTER MODELS

## 3.1 Concrete Surface Temperature and Time of Wetness (Heat Transfer Model)

To perform a sorptivity-based estimate of concrete service life, it is necessary to know when and for how long the concrete pavement or bridge deck is wet.  Thus, a precursor to developing the specific service life models was to develop a heat transfer model for a concrete pavement or bridge deck.  The basic one-dimensional model for heat transfer within a concrete pavement or bridge deck has been presented previously.(9)  Figure 8 shows the basic concrete pavement and bridge deck configurations considered by the model, along with the relevant modes of heat transfer within the concrete and to/from its exposed surfaces.(9,10)  In the final version of the CONCLIFE software, the user has the option of changing the dimensions or the fixed temperature at the bottom soil surface to better model a specific system of interest.(1)  The computer model considers heat transfer by conduction, convection, and radiation.  For radiation to the sky, the sky temperature is estimated based on a series of equations first presented by Walton(11) and detailed below.  Default material properties for the concrete and soil layers(12) are provided in table 7.  In the final version of CONCLIFE, the user also has the option of altering these values if more specific information is available, essentially creating their own weather datafiles.(1)  Environmental data for the heat transfer model is taken from the Typical Meteorological Year (TMY2) weather data files provided by the National Renewable Energy Laboratory.(13)  These files provide typical weather data including ambient relative humidity, ambient temperature, cloud cover, dewpoint temperature, incident global horizontal solar radiation, precipitation events, and wind speed.

Both systems shown in figure 8 are modeled with a one-dimensional finite difference grid with a default spatial resolution of 20 mm.  Four modes of heat transfer are considered at the top concrete surface: conduction into the concrete, convection, solar absorption, and grey-body irradiation to the surroundings.  For conduction, the heat flow contribution (in W/m2) is given by:

Qcond=kconc∗(T0−T1)Δx		(2)

where kconc is the thermal conductivity of the concrete in W/(m oC), T0 and T1 are the surface temperature and temperature at the first internal node, respectively, and Δx is the node spacing

(0.02 m).  For the convection term at the top surface, the heat flow is given by:

Qconv=hconv∗(T0−Tambient)	(3)

where Tambient is the ambient temperature and hconv is the convection coefficient in W/(m2 oC).

Figure 8. Basic configuratins of one-dimensional heat transfer models for concrete pavements and bridge decks.

Table 7. Generic mterial properties for the heat transfer model.

| Material | Heat Capacity (J/(kg oC)) | Thermal Conductivity (W/(m oC)) | Density (kg/m3) |
| --- | --- | --- | --- |
| Concrete | 1000 | 1.5 | 2350 |
| Soil | 800 | 0.3 | 1600 |

While several empirical relationships to estimate convection coefficients exist, for this study the convection coefficient was calculated based on the wind speed available in the weather data files and the following equations used in the commercially available FEMMASSE system:(14)

hconv=5.6+4.0vwind for vwind≤5 mshconv=7.2∗vwind0.78 for vwind> 5 ms	(4)

where vwind is the measured wind speed in m/s.  For radiation absorbed from the incoming sunlight, the heat flow contribution is given by:

Qsun=γabs∗Qinc		(5)

where Qinc is the incident solar radiation from the TMY2 datafile (W/m2) and γabs is the solar absorptivity of the concrete (default value of 0.65).  For the top surface, finally, the irradiation heat loss to the sky is given by:

Qsky=σ ε ∗(T0K4−Tsky4)	(6)

where σ is the Stefan-Boltzmann constant (5.669 * 10-8 W/( m2 oC)), ε is the emissivity  of the concrete (assumed to be 0.9), T0K is the concrete surface temperature in K, and Tsky is the calculated sky temperature, also in K.  The sky temperature was estimated based on an algorithm presented by Walton(11) using the following series of equations:

Tsky=εs14 ∗ Tambient T in K	(7)

where the sky emissivity, εs, is given by:

εs=0.787+0.764*ln(Tdew273)∗Fcloud	(8)

where Tdew is the dewpoint temperature in K taken from the TMY2 datafile, and with the cloud cover factor, Fcloud, as:

Fcloud=1.0+0.024N−0.0035N2+0.00028N3	(9)

where N is the “tenths cloud cover”, taking values between 0.0 and 1.0, and also available in the TMY2 datafiles.

The time step in the finite difference scheme is established based on the discretized element thickness (0.02 m) and the thermal properties of the materials, to ensure numerical convergence of the solution.(15)  The ambient environmental conditions at any specific time are calculated by linear interpolation of the hourly values available from the TMY2 weather files.

Based on these equations, the environmental inputs, and the concrete material properties, the computer model predicts the concrete surface temperature (see figure 9 for an example) and logs wetting and freezing events for the concrete surface.  During the middle of a sunny day, the concrete surface temperature will rise above the ambient temperature due to the incoming solar radiation.  Occasionally, on a clear night, the concrete surface temperature will fall below the ambient value, due to radiation emitted to the night sky. Wetting may be due to a precipitation event or condensation that occurs when the concrete surface temperature drops below the current dewpoint temperature.  Each wetting event is characterized by a starting time, a concrete surface temperature, an external RH prior to wetting, and a duration.  Each freezing event is characterized by a starting time, a minimum temperature achieved during freezing, and a duration.  Figure 10 shows plots of the wetting events for concrete pavements in Kansas City, MO and Providence, RI.  Clearly, the Rhode Island environment is wetter (776 total h wet during the year, vs. 448 for Kansas City).  These wetting and freezing event files are then used in the concrete service life models to be described next.

Figure 9. Temperature predictions for a concrete pavement in Providence, Rhode Island in the spring.  Time indicates cumulative hours from beginning of year.

Figure 10. Plots of wetting events in (top) Kansas City, MO and (bottom) Providence, RI, both for concrete pavements.

## 3.2 Sulfate Attack

The service life model for sulfate attack is based on the model developed by Atkinson and Hearne.(16)  While their development considered the main mode of sulfate ion transport into the concrete to be by diffusion, here we will develop a similar model for sulfate ions transported via sorption from the external environment.  The basic equation developed by Atkinson and Hearne is:(16)

Xspall=2αγf(1−v)E(β CE)2)		(10)

where

CE = concentration of reacted sulfate as ettringite (mol/m3)

E = Young’s modulus (GPa)

Xspall = concrete spalling depth (m)

α = roughness factor for fracture path (default value of one)

β = linear strain caused by reaction of sulfate ions to form one mole of ettringite (m3/mol, default

value of 1.8*10-6)

γf  = fracture surface energy of concrete (N/m)

ν = Poisson’s ratio of concrete (e.g., 0.3)

The basic assumption of this model is that deleterious expansion and cracking is due to the formation of expansive ettringite within the concrete.  When the strain produced by the growing ettringite crystals exceeds the fracture energy of the concrete, failure occurs, as a layer Xspall thick spalls from the concrete surface.  For a sorptivity-based model, the buildup of ettringite is considered to be due to external sulfate ions penetrating into the concrete along with the sorbed external solution.(3) To use this model, the user must specify the concentration of sulfate ions in the external solution (e.g., rainwater or groundwater) and the sorption properties of the concrete.  Specifically, for each wetting event, the CONCLIFE program calculates a penetration depth based on the duration of the event, the concrete sorptivity, and the environmental conditions (RH and concrete surface temperature).  The measured sorption coefficients are adjusted for the RH just prior to the wetting event, using linear interpolation and assuming a sorptivity value of zero at 100 percent RH (saturated) conditions.  They are further adjusted for the concrete surface temperature based on the physical properties (viscosity and surface tension) of water as a function of temperature.(10)  Assuming that sorptivity scales as (σ/η)1/2,(10) where σ is surface tension (expressed in units of kg/(m.s) x 10-4)(17) and η is viscosity (in units of dynes/cm)(15), one finds:

ση=2.054+0.0334∗T−0.000085∗T2	(11)

where T is expressed in oC.

Based on these adjusted sorption coefficients, the concrete internal “sulfate (ettringite) concentrations” down to the penetration depth are updated and equation 10 is used to evaluate whether or not new spalling will occur.  If so, the spalling depth is updated.  This process is repeated until the spalling depth exceeds the user-specified failure criteria, indicating the estimated service life for the concrete. This model comprises one of the two main user screens of the CONCLIFE program.(1)

## 3.3 Freeze/thaw Damage

The service life model for freeze/thaw deterioration is based on the critical air void saturation concept of Fagerlund.(18)  The basic assumption is that the air voids in field concrete are slowly filled by liquid water during environmental exposure.  This “filling” rate is assumed to be equivalent to the later age sorption coefficient (after the nick point time) discussed above.  When a critical fraction of these air voids have become saturated (water-filled), the next freeze/thaw cycle will cause damage to the concrete.  For the purposes of the model developed in CONCLIFE, failure is characterized by the time necessary to achieve the critical saturation.  The subsequent cracking developed due to cyclic freezing and thawing is not considered.  Critical parameters are the porosity and air void content of the concrete and its sorption characteristics.  To implement this model in the CONCLIFE program, each wetting event is examined in turn.  If the duration of the wetting event exceeds the nick-point time, the penetration depth is computed based on the sorption coefficients and the concrete porosity.  The sorption occurring after the nick-point time is used to update the saturation of the air voids within this penetration depth.  If the saturation at some depth is greater than the user-specified critical saturation, spalling occurs.  Once again, when the cumulative spalling exceeds the user-specified failure criteria, an estimate of the concrete service life is achieved.  This model comprises the second main user screen within the CONCLIFE program.(1)

# CHAPTER 4: SUMMARY

The technical basis for the CONCLIFE program has been presented.  Both experimental and computational research have played major roles in the development of the CONCLIFE package.  This combined experimental/computer modeling approach is viewed as the most fruitful avenue for advancing the science of service life prediction of concrete structures.

# ACKNOWLEDGEMENTS

The authors would like to thank the four state Departments of Transportation for providing concrete core samples for this study.  They would also like to thank Mark Felag of the Rhode Island Department of Transportation for useful discussions, Dr. George Walton of BFRL for useful discussions concerning the concrete heat transfer model, and Prof. Doug Hooton of the University of Toronto for providing an advanced draft of the proposed sorptivity test standard which greatly expedited the process of preparing a test for balloting by ASTM C09.

# REFERENCES

- Ehlen, M.A., and Bentz, D.P., “Service Life Prediction for Concrete Pavements and Bridge Decks Exposed to Sulfate Attack and Freeze-Thaw Deterioration. Volume I: CONCLIFE User’s Manual,” FHWA report, 2001.

- ASTM draft sorptivity test.

- Bentz, D.P., Clifton, J.R., Ferraris, C.F., and Garboczi, E.J., “Transport Properties and Durability of Concrete: Literature Review and Research Plan,” NISTIR 6395, U.S. Department of Commerce, September 1999.

- ASTM C215, “Standard Test Method for Fundamental Transverse, Longitudinal, and Torsional Resonant Frequencies of Concrete Specimens,” ASTM C215-97, Vol. 04.02, 1999.

- ASTM C1202, ASTM C1202-   , Vol. 04.02, 1999.

- “Recommendation of TC 116-PCD: Tests for Gas Permeability of Concrete C. Determination of the Capillary Absorption of Water of Hardened Concrete,” Materials and Structures, Vol. 32 (217), 178-179, 1999.

- Howe, S., “The Great Tape Off,” Backpacker, Vol. 29 (190-8), 59, 2000.

- Martys, N., and Ferraris, C.F., “Capillary Transport in Mortars and Concretes,” Cement and Concrete Research, Vol. 27 (5), 747-760, 1997.

- Bentz, D.P., A Computer Model to Predict the Surface Temperature and Time-of-Wetness of Concrete Pavements and Bridge Decks, NISTIR 6551, U.S. Department of Commerce, August 2000.

- Bentz, D.P., Ehlen, M.A., Ferraris, C.F., and Garboczi, E.J., Sorptivity-Based Service Life Predictions for Concrete Pavements, 7th International Conference on Concrete Pavements, Orlando, FL, September 2001.

- Walton, G.N., Thermal Analysis Research Program- Reference Manual, NBSIR 83-2655, U.S. Department of Commerce, March 1983, Update 1985.

- McCullough, B.F., and Rasmussen, R.O., Fast-Track Paving: Concrete Temperature Control and Traffic Opening Criteria for Bonded Concrete Overlays, Volume 1: Final Report, FHWA-RD-98-167, Federal Highway Administration, 1997.

- Marion, W., and Urban, K., User’s Manual for TMY2s- Typical Meteorological Years, National Renewable Energy Laboratory, June 1995.

- Schlangen, E., Online Help/Manual module HEAT of FEMMASSE, 1990-2000, FEMMASSE b.v., The Netherlands, 2000.

- Holman, J.P., Heat Transfer (McGraw-Hill Book Company, New York, 1981).

- Atkinson, A., and Hearne, J.A., Mechanistic Model for the Durability of Concrete Barriers Exposed to Sulphate-Bearing Groundwaters, MRS Symposium Proceedings, Vol. 176, 149-156, 1990.

- Weast, R.C. (ed.), CRC Handbook of Chemistry and Physics, 63rd edition, 1983.

- Fagerlund, G., Modeling the Service Life of Concrete Exposed to Frost, International Conference on Ion and Mass Transport in Cement-Based Materials, University of Toronto, October, 1999.

# APPENDIX A: ASTM CXXXX Proposed Test Method for Measurement of Rate of Absorption of Water by Hydraulic-Cement Mortars or Concretes

(DRAFT- Under ballot but not yet approved by ASTM)

## Scope

1.1	This test method covers the measurement of the rate of absorption (sorptivity) of water by hydraulic cement mortar or concrete, by measuring the increase in the mass of a specimen resulting from the absorption of water as a function of time when only one surface of the specimen is exposed to water.  Two procedures are described. In procedure A, the specimen is supported on top of water and the water ingress is by capillary suction. In procedure B, the water is placed on top of the specimen (ponding) and gravity also plays a role in the water ingress.

1.2	This standard does not purport to address all of the safety concerns, if any, associated with its use. It is the responsibility of the user of this standard to establish appropriate safety and health practices and determine the applicability of regulatory limitations prior to use.

1.3	The values stated in SI units are to be regarded as the standard.

## Referenced Documents

C 642 Standard Test Method for Density, Absorption, and Voids in Hardened Concrete

## Significance and Use

  - The resistance of concrete subjected to many aggressive environments is a function to a

large extent of the penetrability of the pore system.  In unsaturated concrete, the rate of ingress of water or other liquids is largely controlled by capillary rise absorption.  This method is based on that developed by Hall () who called the phenomenon “water sorptivity”.

  - The water absorption of the concrete or mortar surface varies with (a) concrete mixture

proportions including the addition of chemical admixtures and supplementary cementitious materials, (b) surface finishing, (c) entrained air content, (d) type and duration of curing, (e) age, (f) degree of hydration, and (g) surface treatments such as sealers, form oil, etc. Also, the water absorption is strongly affected by the moisture condition of the concrete tested.

  - In general, the exposed surface of concrete may be different in absorption from the

interior.  The surface is the area exposed to the most potentially adverse conditions.  This test method can measure the water absorption rate both of the concrete surface and of the interior. The specimen can be a section of a core taken at different depths from the surface.

  - This method is different from the test described in ASTM C642 in the procedure to

expose the specimens to water. In C 642 the specimens are oven dried and then immmersed completely in water first at 21 C and then boiled under water for 5 h. In the test described here only one surface is exposed to water while the others are protected from the environment. This simulates the water absorption in a wall in contact on one side with water, while the C 642 test is used to determine the maximum amount of water that can be absorbed in a specimen.

## Apparatus

4.1	Pan - A watertight polyethylene or other corrosion-resistant pan large enough

to accommodate the test specimen with the surface to be tested exposed to water.

4.2	Support Device - Rods, pins, or other devices, made of materials resistant to corrosion by water or alkaline solutions, which allow free access of water to the test surface of the test specimen during the test.  Alternately, the sample can be supported on several layers of blotting paper or filter papers with a total thickness of at least 1 mm.

4.3	Top-pan Balance - with sufficient capacity for the test specimens and accurate to at least 0.1 g.  The balance should comply with ASTM C1005.

4.4	Timing Device- Stop watch or other suitable timing device accurate to 1 s.

4.5	Tissue Paper or Cloths - for wiping excess water from specimen surfaces.

4.6	Environmental Chamber - the chamber should have a fan and should be able to maintain a temperature of 50 ± 2C and a relative humidity at 80%  3 %. Alternatively, an oven able to maintain a temperature of 50 ± 2C and a dessicator can be used. The relative humidity (RH) is controlled in the dessicator with a salt solution of potassium bromide. The dessicator needs to be large enough to contain the specimens to be tested.

4.7	Polyethylene Storage Container - with sealable lid, which is large enough to contain a test specimen. The container should not have a volume larger than 5 times the specimen volume. An option for the container could be to have lock valves in the lid that could be connected to a system to measure the RH inside the container.

## Reagents and Materials

  - Potassium bromide, reagent grade (Note 1).

Note 1: Only required if the oven/dessicator described in 4.6 is used.

## Test Specimens

6.1	Use, as the standard test specimen, a 100 mm ± 6 mm diameter core or cylinder, and a length of 50 ± 3 mm. The cross section of the specimen should be constant ( 5 mm2).  Measure the actual diameter of the specimen for use in calculations by averaging at least 4 diameters.  For tests to evaluate curing effectiveness, take cores from the central portion of slabs at least 30 mm from any edge.

6.2	Test a minimum of two specimens.

6.3	Since water absorption is affected by curing, conduct replicate tests on specimens having test surfaces at the same depth with respect to the exposed surface.

## Sample Conditioning

7.1	Place test specimens in the environmental chamber, that is at a temperature at 50 ± 2C and RH at 80%  3 %, for 3 days. Alternatively, place test specimens in a dessicator inside an oven which is able to maintain a temperature of 50 ± 2C. Control the relative humidity in the dessicator with a saturated solution of potassium bromide. Do not allow test specimens to come in contact with the saturated salt solution.

  - Place specimen on support device inside the sealable polyethylene container.

  - Place the container at 23C  ± 2C in an environmental chamber or oven for 15 days

(Note 2).

Note 2:	The conditioning inside the sealed container results in equilibration of moisture distribution within the test specimens and has been found to provide internal relative humidities of 50 to 70%.  This is similar to the relative humidities found in field structures (,).

7.4	Store the specimen in the desiccator jar or a sealable polyethylene container until test.

## Procedure

8.1	Conduct the absorption procedure in 8.6 to 8.9 at 23 ± 2C with tap water conditioned to the same temperature. If the experiment is continued for more than 3 days, saturated limewater shall be used instead of tap water. The limewater shall be prepared by dissolving sufficient calcium hydroxide (Ca(OH)2) in distilled water to exceed the saturation concentration (1.65 mg/g of water).

8.2	Remove the specimen from the container or bag and measure the mass of the conditioned test specimen to the nearest 0.1 g prior to sealing of side surfaces.  Record this mass.

8.3	Seal the sides of test specimens with a bituminous, epoxy, or other coating to prevent absorption of water into the sides and to prevent evaporation of internal water (Note 3). Also cover the top of the specimen with the same material or with a bag attached with a rubber band.

Note 3: Strips of impermeable sheets, bituminous sheet, epoxy paint, vinyl electricians’ tape, duct tape, or aluminum tape have been found to be effective for this purpose.

  - Again measure the mass of the specimen with sides and the non tested surface sealed

and record as the initial mass for rate of absorption calculations.

  - PROCEDURE A: Absorption by capillary

8.5.1	Fill the pan with tap water or limewater (see 8.1) until the level is 1 to 3 mm above the top of the support device.

8.5.2	Record the time and immediately place the test surface of the specimen on the support device (see Figure 11).

    - After 60 ± 2 s, remove the test specimen from the container, stop the stopwatch,

blot off any surface water with a dampened tissue or cloth, and measure the mass within 15 s.

    - Immediately replace the test surface of the specimen on the support device in

contact with water and start the stopwatch

    - Repeat the procedure in 8.5.3 and 8.5.4 after total elapsed contact times of

5, 10, 20, 30, and 60 min (± 10 s) from first contact of the specimen with water. Continue the measurements every hour up to 6 h and once a day up to 7 days from the first contact of the specimen with water. After blotting, dry the surface of the specimen, and invert the specimen so that the wet surface does not come in contact with the balance pan.

Note 4: For measurements after the first 10 min, stopping the stopwatch while the specimen is not in contact with the water is not necessary.

Figure 11. Schematic of Procedure A.

8.6 PROCEDURE B: Absorption by ponding

8.6.1	This method allows the measurement of absorption where the surface exposed to the water is the top surface. Thus, gravity will be an additional force to accelerate the penetration of the water into the specimen. Depending on the end use application of the concrete, absorption either against or with gravity may be a more appropriate measure. For example, for concrete pavements, absorption with gravity is perhaps more relevant.

8.6.2	Use strip caulk and duct tape to build a dam around the edge of the top of the specimen. Make sure that the caulk adheres tightly to the specimen. The dam should be about 10 mm in height.

Note 5 : If the dam is built in such a way that it does not lay on the top of the specimen, the

test surface is equal to the top section of the specimen.

8.6.3	Again, determine the mass of the specimen with sides and bottom sealed, and with the dam on the top side. Record this value as the initial mass for rate of absorption calculations.

8.6.4 	Fill the dam on top of the specimen with tap water up to the top of the dam and immediately record the time.

8.6.5	After 60 ± 2 s, pour the water out of the test specimen, stop the stopwatch, and blot off any surface water with a dampened tissue or cloth and measure the mass within 15 s.

    - Immediately refill the dam on top of the specimen with water and restart the

stopwatch.

8.6.7	Repeat steps 8.6.5 and 8.6.6 after total elapsed contact times of 5, 10, 20, 30, and 60 min (± 10 s) from first contact of the specimen with water. Continue the measurements every hour up to 6 hours and once a day up to 7 days from the first contact of the specimen with water.

Note 6: To avoid evaporation of the water when the measurements are longer than one hour, cover the specimen loosely with plastic wrap.

Figure 12. Schematic of Procedure B.

## Calculations

9.1	The initial rate of absorption, I, is the change in mass (g) divided by both the cross-sectional area of the test specimen (mm2) and the density of water at the temperature recorded. (Note 7)

Note 7. The density of water depends on its temperature. However, the effect of this variation with the temperature is not significant in this procedure, so the temperature measurement is not required.  The density of the water could be assumed to be 1.00 g/mL (0.001 g/mm3).

9.2	The initial water absorption (mm/min½) is defined as the slope of the line of I plotted against the square root of time (min½).  Obtain this slope after using least-squares, linear regression to establish the plot of I vs. time½.  Do not include the origin (measurement at 1 min) as a datum point (Note 7). Use all the points in the regression until the plot shows a clear change of slope. If no portion of the curve I vs. time½ data is linear (a regression coefficient of less than 0.98) and the data show some systematic curvature, absorption cannot be determined. An example is given in the Appendix.

Note 8. , The initial change in mass up to one minute is often higher than for subsequent time intervals in part because it corresponds to water absorbed on the outer surface in contact with the water and not absorbed inside the specimen (in the pores).

9.3 Obtain the water absorption at later age (after the line plotted in 9.2 shows a change in slope) using least-squares, linear regression to determine the slope of the second portion of the plotted points for I vs. time½. Include only points for times from 1 day to 7 days. If no portion of the curve I vs. time½ data is linear (a regression coefficient of less than 0.98) and shows some systematic curvature in the region, absorption at later age cannot be determined.

## Report

  - An example report is given in the Appendix 1.

  - Report the following:

10.2.1 Date sampled or date cast;

10.2.2 Source of sample;

10.2.3 Relevant background information on sample such as mixture proportions, curing

history, type of finishing, and age, if available;

10.2.4 Dimensions and dry mass of the test specimen;

10.2.5 A plot of the absorption vs. square root of time;

10.2.6 The average initial water absorption calculated to 0.1 mm/min½  and the

individual absorption rates for the two specimens.

10.2.7 If the initial water absorption could not be derived from all the data points as

discussed in 9.2, indicate which data points are omitted.

10.2.8  Report the time (hours) at which the slope of the linechanges.

10.2.9 The average later age water absorption calculated to 0.1 mm/min½ and the

individual absorption rates of the two specimens tested.

    - If the later age water absorption could not be derived from all the data points

as discussed in 9.3, indicate which data points were omitted.

## Precision and Bias

11.1	Precision - The precision of this procedure has not yet been determined.

11.2 Bias - Since there is no accepted reference material suitable for determining the bias of this procedure, no statement on bias is made.

Keywords:   rate of absorption, initial water absorption, concrete, mortar, permeability.

## APPENDIX 1:Example Rate of Absorption Test

Cast Date: 3/2/99     Test Date:  3/14/00

Sample No. F-68 				Concrete Mixture: 35% fly ash / w/cm = 0.45

- Sample Conditioning:  Cast, steam cured, test face =top surface

Sample:  Age  378 days			Age at coring: NA

Mass of Conditioned disc:  750.5 g (prior to sealing sides)

Diameter (mm):  101.6			Area:  8107.1 mm2

- Thickness (mm):  50.8

- Water temp:  20.7oC

| Test Time |  | Time | Mass | Mass | Mass/area = I |
| --- | --- | --- | --- | --- | --- |
| Days | min | [min½] | [g] | [g] | [mm] |
|  | 0 | 0.0 | 761.83 | 0.00 | 0.0000 |
|  | 1 | 1.0 | 762.45 | 0.62 | 0.0765 |
|  | 5 | 2.2 | 762.46 | 0.63 | 0.0780 |
|  | 10 | 3.2 | 762.48 | 0.65 | 0.0805 |
|  | 20 | 4.5 | 762.50 | 0.67 | 0.0826 |
|  | 30 | 5.5 | 762.57 | 0.74 | 0.0913 |
|  | 60 | 7.7 | 762.63 | 0.80 | 0.0987 |
|  | 120 | 11.0 | 762.68 | 0.85 | 0.1048 |
|  | 180 | 13.4 | 762.73 | 0.90 | 0.1110 |
|  | 240 | 15.5 | 762.77 | 0.94 | 0.1159 |
|  | 300 | 17.3 | 762.81 | 0.98 | 0.1209 |
|  | 360 | 19.0 | 762.82 | 0.99 | 0.1221 |
|  | 420 | 20.5 | 762.84 | 1.01 | 0.1250 |
| 1 | 1537 | 39.2 | 763.05 | 1.22 | 0.1505 |
| 2 | 3220 | 56.7 | 763.12 | 1.29 | 0.1591 |
| 3 | 4475 | 66.9 | 763.15 | 1.32 | 0.1628 |
| 4 | 8793 | 93.8 | 763.39 | 1.56 | 0.1924 |
| 7 | 10370 | 101.8 | 763.45 | 1.62 | 0.1998 |
| 8 | 11540 | 107.4 | 763.48 | 1.65 | 0.2035 |
| 9 | 13225 | 115.0 | 763.58 | 1.75 | 0.2159 |

- EQUATION OF LINE:

- Initial Absorption

I = S t + b. (points measured during the first day are used, excluding the point at origin)

S =  2.63 x 10-3 mm/min.	b = 0.741 x 10-2 		r =  0.98

- Later age Absorption

I = S t + b. (points measured after the first day are used)

S =  0.877 x 10-3 mm/min.	b = 0.11 x 10-2 		r =  0.98

? Certain commercial products are identified to completely specify the research program.  In no case does such identification imply endorsement by NIST or FHWA, or that the identified products are the best available for the purpose.

? This proposed test method is under the Jurisdiction of ASTM Committee C-9 on Concrete and Concrete Aggregates and is the direct responsibility of Subcommittee C09.66 on Resistance to Fluid Penetration.

? C. Hall, “Water Sorptivity of Mortars and Concretes: A Review”, Magazine of Concrete Research. Vol. 41, No. 147, June 1989, pp. 51-61.

? DeSouza SJ, Hooton RD, Bickley JA, “Evaluation of laboratory drying procedures relevant to field conditions for concrete sorptivity measurements,” Cement Concrete Aggr, Vol. 19, No. 2, Dec 1997, pp. 59-63.

? DeSouza SJ, Hooton RD, Bickley JA,  “A field test for evaluating high performance concrete covercrete quality,” Can J Civil Eng, Vol. 25, No. 3, Jun 1998, pp. 551-556.